CATEGORY 400

STRUCTURES

SECTION 421 — REINFORCING STEEL

421.02 MATERIALS

DELETE:

Galvanizing 									A153

INSERT:

Galvanizing

Reinforcing Steel   			A123

Hardware		A153

421.03 CONSTRUCTION.

DELETE:  421.03.06 Splicing in its entirety.

INSERT:  The following.

421.03.06 Splicing.  Furnish bars in the lengths and have been spliced as specified and as approved in the working drawings.  Do not perform additional splicing without approval.  Make lap splices with the bars in contact and wired together.  Do not weld reinforcing steel or weld attachments to reinforcing steel without approval. Perform welding per AWS D1.4.