CATEGORY 400

STRUCTURES

SECTION 435 — CLEANING AND PAINTING

NEW STRUCTURAL STEEL

435.01.01 Areas to be coated.

(b)	Weathering Steel.

ADD:  The following after (4).

(5)	All steel surfaces when specified.  Refer to 436.01.01(a)

435.01.04 Definition of Bridge.

DELETE:  435.01.04 in its entirety.

INSERT:  The following.

435.01.04 Minimum Contracting Requirements for Shop Painting.  To be eligible to perform the work of removing and applying paint in a shop environment, certification as specified in (a) or (b) is required.  All certificates shall be effective prior to Award of Contract and shall remain in effect for the duration of the Contract.  Refer to 436.01.03.

- SSPC-QP3.  Standard Procedure for Evaluating of Qualifications of Painting Contractors; Shop Application to Complex Structures.

- AISC 420-10.  Certification Standard for Shop Application of Complex Protective Coating Systems.

435.01.05. Definition of Bridge.  Refer to 436.01.04.

435.02 MATERIALS.

435.02.01 Paint Systems.

DELETE: The second paragraph “New Steel (Includes New Structures, Repairs, and Widenings).” in its entirety.

INSERT:  The following.

New Steel (Includes New Structures, Repairs, and Widenings).  The paint shall meet Paint System B.  Touch up paint for the shop primer prior to Coats II and III shall conform to Coat I of Paint System C as approved by the coating manufacturer.  The color of the finish coat shall match ACS-STD-595A, exact color as specified.

435.03 CONSTRUCTION.

435.03.06 Field Cleaning and Painting.

ADD:  The following at the end of the first paragraph.

Follow the stripe coat schedule per 436.03.21.

DELETE:  435.03.16 Time Restrictions for Field Painting, in its entirety.

INSERT:  Restrictions for Shop and Field Painting.

- Apply shop paint at any time in an enclosed facility under controlled environmental conditions and in accordance with the manufacturer’s recommendations.

- For field painting, refer to 436.03.20.

DELETE:  435.03.17 Weather Restrictions for Painting, in its entirety.

INSERT:  The following.

435.03.17 Weather Requirements for Painting.  Refer to 436.03.19.