CATEGORY 400

STRUCTURES

SECTION 436 — CLEANING AND PAINTING

EXISTING STRUCTURAL STEEL

436.01 DESCRIPTION.

436.01.03 Minimum Contracting Requirements for Field Painting.

DELETE:	(a) in its entirety.

INSERT:	The following.

(a)	Standard Procedure for Evaluating Qualifications of Painting Contractors: Field Application to Complex Structures. The Society for Protective Coatings (SSPC) QP-1 Certified Applicator Specialist (CAS) requirements are waived.

436.02 MATERIALS.

DELETE:	436.02.02 Abrasives, in its entirety.

INSERT:	The following.

436.02.02 Abrasives.  Provide material safety data sheets (MSDS) for the abrasives and a letter, from the abrasive supplier, indicating that expendable abrasives meet SSPC-AB 1 and recyclable abrasives meet SSPC-AB 3.  Verify the cleanliness of recycled abrasives per SSPC-AB 2.

436.03 CONSTRUCTION.

436.03.01 Submittals.

DELETE:	(a) in its entirety.

INSERT:	The following.

- Copy of SSPC-QP Certification.  Refer to 435.01.04 for shop painting and 436.01.03 for field painting.

436.02 Personnel Qualifications and Responsibilities.

DELETE:	(c) in its entirety.

INSERT:	The following.

- Certified Industrial Hygienist (CIH) or Certified Safety Professional (CSP).  When the work includes the disturbance or removal of paint containing toxic metals, ensure an approved CIH or CSP is present when the work is performed.  Submit to the Engineer documentation that the CIH or CSP has the following.

- Valid certification by the American Board of Industrial Hygiene or Board of Certified Safety Professionals.

- Field sampling and oversight experience involving removal of paint that contains toxic metals from structures.

- Errors and omissions insurance coverage of not less than $1,000.000.00 for the type of work specified.

All field sampling and testing shall be performed by the CIH or CSP or by an employee working under direct supervision of the CIH/CSP, and shall be witnessed by the Engineer.  Notify the Office of Structures Inspection and Remedial Engineering Division at least 24 hours prior to sampling and testing.

The CIH or CSP shall review all results of sampling and testing performed on the project.  The CIH or CSP or a person working under their direction, shall prepare written reports interpreting these results for compliance to the applicable regulations.  Submit a copy of reports and analysis to the Engineer within five working days after sampling.

Submit a written certification within five days after the end of each month stating compliance with the plans of Action and Compliance Programs specified for worker protection, environmental protection, and waste handling have occurred and all deficiencies found have been addressed.  The certification shall be prepared and signed by the CIH or  CSP or a person working under their direction.

436.03.03 Quality Control (QC) Plan, Inspection Procedures, and Recording Systems.

DELETE:	The last paragraph, “Maintain on site…on site audits.”

INSERT:		The following.

Maintain on-site copies of the daily job quality control records and make available to the Engineer upon demand.  Submit records from on-site audits and inspections from SSPC, MOSH, OSHA, EPA, and MDE.

436.03.04 Inspection Equipment.

ADD:	After (q).

(r)	Dry film thickness calibration plates traceable to the National Institute of Standards and Technology.

(s)	Measuring stick or pole to measure platform under clearance.  The stick or pole shall be collapsible and have a minimum measuring height of 20 ft.

436.03.10 Methods of cleaning.

DELETE:	The table.

INSERT:	The following table.

| PAINT SYSTEM | SUBSTRATE | METHOD OF CLEANING |
| --- | --- | --- |
| C & D | Abrasive Blast Cleaned Steel | Existing Paint to be Removed - Localized (a) and (b) and complete (h) |
| E & H | Overcoating Existing Paint | Existing Paint to be Overcoated - Localized (a) and complete (c) followed by (d) and (e) |

DELETE:	(h)	Near White Metal Abrasive Blast Cleaning, in its entirety.

INSERT:	The following.

(h)	Near White Metal Abrasive Blast Cleaning.  Do not use steel shot in the field.  When using steel shot in the shop, add the appropriate amount of steel grit and maintain the mixture to produce an etched surface texture and not the peened surface texture that results when blast cleaning with shot alone. The end surface condition shall meet SSPC-SP 10, Near White, and as depicted in SSPC Vis 1.  Ensure that abrasives are dry and free of oils, grease, and other harmful materials, such as lead dust, at the time of use.  Abrasive media shall produce blasted surfaces having a surface profile height of 1.5 to 4.0 mils as determined per D 4417 Method C.

Whenever the existing condition causes surface profile to exceed 4 mils on weathering steel and in heavily corroded areas of existing structural steel members, apply at least two coats of primer to achieve the minimum dry film thickness specified above the profile.

436.03.15 Surface Condition Prior to Painting.

ADD:  After the last paragraph, “Prior to the…cleaned as specified.”

Move all hooks, cables, beam clamps, and outriggers during cleaning operation to allow the underlying surfaces to be cleaned.  Any containment attachments that cannot be moved during cleaning and painting must be power tool cleaned to SP-11 Bare Metal and coated using Paint System H.

DELETE:	436.03.17 Paint Representative, in its entirety.

INSERT:	The following.

436.03.17 Paint Representative.  The representative shall be a technical representative of the paint manufacturer.  During initial execution of the work the Engineer may require the paint representative to be on site to approve with the Engineer the degree of cleanliness prior to painting and the method of application of the coating system.  The Engineer may stop paint operations for failure to meet this requirement regardless of the reason for failure.  Areas cleaned prior to ceasing paint operations shall be recleaned if required.

DELETE:	436.03.19 Time Restrictions for Field Painting in its entirety.

INSERT:	The following.

436.03.19 Weather Requirements for Painting.  All surfaces to be painted shall be sound and cleaned as specified.  Painting is allowed when:

- There is no presence of rain, snow, fog, or mist dampening or condensing on the surface.

- The relative humidity does not exceed the maximum humidity specified by the paint manufacturer.

- The ambient temperature in the shade is above 40 F.

- The surface temperature is above 35 F or the minimum temperature specified by the manufacturer, whichever is greater, and will be constant or higher until the paint cures to readiness for recoating.

- The surface temperature is a minimum of 5 F above the dew point until cure or intermediate coats have been top coated.

- The surface temperature is below 120 F or the temperature recommended by the paint manufacturer, whichever is less.

Whenever it is suspected that moisture is condensing upon the surface, the psychrometer will be used to check dew point, etc. If the conditions measured by the psychrometer are marginal, the Engineer may permit a well-defined area of the surface to be lightly moistened with a damp cloth and observed.  If the dampness evaporates within 15 minutes, the surface will be considered satisfactory for the application of paint.  Regardless of any environmental test results, when fresh paint is damaged, replace or repair the paint at no additional cost to the Administration.

Schedule the operations so that all cleaned surfaces are painted within 24 hours.  If rust bloom appears or the air or steel temperature falls below five degrees above the dew point after cleaning and prior to application of the primer coat, reclean the affected areas to the satisfaction of the Engineer at no additional cost to the Administration.

DELETE:	436.03.20 Weather Restrictions for Painting, in its entirety.

INSERT:	The following.

436.03.20 Artificial Climate Controls.

- Minimum temperature (substrate, air, and material) and all other environmental restrictions shall be maintained as specified.  Refer to 436.03.19.

- If heat is to be used to reach environmental conditions, use only an indirect heat source that will disperse the heat evenly throughout containment area.

- Heat shall be maintained in accordance with the manufacturer’s recommendations or time at recoat, whichever is greater, 	after the coating is completed in the desired areas.

- Install an operational automatic temperature data recorder inside the containment area until time to recoat, or manufacturer’s recommendations, whichever is greater.  The placement will be determined by the Engineer.

- Artificial Climate Controls will be at no additional cost to the Administration and no additional time will be added to the contract.

- Failure to maintain artificial climate controls will be cause to be denied work until weather dictates that artificial climate controls are not needed.

436.03.21 Application of Prime, Intermediate, and Finish Coats.

ADD:	After the second paragraph “Apply all paint…proper coating thickness.”

Move hooks, cables, beam clamps, and outriggers whenever possible to allow cleaning and application of all three coats of paint to these areas.

ADD:	After the last paragraph “Apply each coat…and the Engineer.”

At project completion, all fascia beams shall have a smooth and uniform appearance throughout.  Should any fascia have runs, sags, heavy film build, blisters, bubbles, orange peel or any other coating defect which does not give the appearance of a smooth uniform surface, reclean and paint specific areas or the entire fascia as directed by the Engineer.

436.03.28 Field Cleaning Containment System Plan Guidelines.

ADD:	The following after (i).

(j)	All steel corrugated decking containment materials shall have either fire retardant plastic, impermeable screen or tarpaulins laid on top to prevent the leaking of grit, dust, toxic metals and debris during blast cleaning activities.

DELETE:	436.03.30 Worker Protection and Exposure Monitoring, in its entirety.

INSERT:	The following.

436.03.30 Worker Protection and Exposure Monitoring.  In addition to complying with all applicable OSHA and MOSH regulations, when the project involves coatings that contain toxic metals, provide the services of a CIH or CSP per 436.03.02(c) and submit a Worker Protection Compliance Program per 436.03.31.  The CIH or CSP, or a technician working under the direction of the CIH/CSP shall monitor worker exposures during paint disturbance operations at each structure and provide worker protection oversight.

Regardless of whether or not toxic metals are present, provide a hand wash station with soap and towels at each work site.  As dictated by the monitoring results and the applicable OSHA standards, provide a cleanup area with a shower, soap, hot and cold potable pressurized water, a change area with a locker, and an approved container for collecting and disposing of waste at each work site.

Ensure that 													the hand wash and shower facilities are available to all site personnel.  Hygiene facilities shall meet 29 CFR 1926.51, Sanitation Standard.

DELETE:	436.03.31 Worker Protection Compliance Program in its entirety.

INSERT:	The following.

436.03.31 Worker Protection Compliance Program. The Worker Protection Compliance Program shall be on company letterhead and meet OSHA and the MOSH - Lead in Construction Standards, and other applicable toxic metal standards.  The Worker Protection Compliance Program shall be reviewed and signed by the CIH or CSP and at least one copy of the submittal shall have an original CIH or CSP seal.  The Worker Protection Compliance Program shall include a commitment for the CIH or CSP, or a person working under the direction of the CIH/CSP, to provide written certification each month of compliance with the Worker Protection Compliance Program, including biological monitoring.  Provide a copy of the letter within 6 working days after the end of each month.

A Worker Protection Compliance Program is not required when the coatings being disturbed do not contain toxic metals.

DELETE:	436.03.33 Environmental Protection Plan of Action (EPPA) in its entirety.

INSERT:	The following.

436.03.33 Environmental Protection Plan of Action (EPPA).  An EPPA confirming that the environment is protected from contamination is required when the coatings are being abrasive blast cleaned (regardless of the presence of toxic metals), or the coating being disturbed contains toxic metals (regardless of the method of preparation).  When an EPPA is required, it shall be reviewed and sealed by a CIH or CSP and shall include procedures for monitoring air, soil, and water.

Include a location plan showing the type and location of high volume ambient air monitors if applicable, and the procedures that will be followed for visible emissions assessments and inspections of the soil, water, surrounding property and structures, and pavement.  Submit 6 copies of each plan signed and sealed by the CIH or CSP.  All submittals shall be in writing and on company letterhead.  At least one copy shall have an original seal.  Address the proposed procedures that will be implemented for the following as defined in 436.03.34:

      - For any paint disturbance using dry methods of preparation, address the daily visual emissions observations that will be performed and the corrective action that will be implemented in the event emissions or releases occur.

      - When paint containing toxic metals is being disturbed, address the provisions for high volume ambient air monitoring (TSP - Monitoring); monitor citing, calibration, and operation; filter handling and shipping; and laboratory analysis, including the name and qualifications of the laboratory. Test results shall be reviewed and summarized by the CIH or CSP. Provide copies to the engineer within 6 work days of sample collection by the CIH or CSP.

      - For any paint disturbance, address the visual assessments for soil, water, and sediment undertaken each day throughout the Contract, together with the proposed cleanup activities. Provide to the Engineer a commitment from the CIH or CSP within 6 work days after the end of the month that certifies compliance with the EPPA.

436.03.34 Methods for Assessing Emissions.

DELETE:	(b)	Ambient Air Monitoring, in its entirety.

INSERT:	The following.

- Ambient Air Monitoring. Unless otherwise directed, ambient air monitoring is required when the coatings being disturbed contain toxic metals, and whenever the paint removal operations are located within 500 ft. of houses, schools, parks, playgrounds, shopping areas, or similar areas of public exposure.  Ensure monitoring starts one half hour before blast cleaning or power tool cleaning begins and continues for the entire duration of the cleaning activity or 7 hours, whichever is greater.

- Abrasive Blast Cleaning.  Daily ambient air monitoring at each structure being abrasive blast cleaned shall begin one day prior to beginning work and during the first 10 days of productive abrasive blast cleaning operations.  When the results indicate that the containment is controlling emissions, full-time monitoring may be discontinued unless otherwise directed.  Ensure monitoring is repeated for 2 consecutive days every month thereafter during the work shift while blast cleaning or other dust producing operations are underway.

When the results of the original 10 days of monitoring or the periodic monthly tests are unacceptable, ensure that monitoring continues full-time. Monthly monitoring may be initiated or resumed only when approved, and only after the results of the testing indicates that the containment is controlling emissions.

Resume full-time monitoring when unacceptable visible emissions or residues are observed on the ground or water and as directed.

- Hand and Power Tool Cleaning. Begin daily ambient air monitoring at each structure one day prior to beginning work and during the first five days of hand tool cleaning and power tool cleaning. When the results indicate that the containment is 	controlling emissions, full-time monitoring may be discontinued unless otherwise                             directed. Resume monitoring when visible residues are observed on the ground or in the water, or visible dust is observed exceeding the visible emissions criteria established above.

- Monitor Placement and Reporting. Place total suspended particulate (TSP) monitors in areas of potential public exposure, including but not limited to adjacent to homes, businesses, parks, and pedestrian walkways, that are within 500 ft. of each project site during cleaning operations in conformance with Method D of SSPC Guide 6. The CIH or CSP shall provide for Engineer acceptance, the proposed monitoring locations in advance, together with the rationale for the selection of each site. All TSP monitoring samples shall be analyzed using Method 40 CFR 50 Appendix B and G by a laboratory approved by the American Industrial Hygiene Association.

The CIH or CSP shall use an Adjusted Daily Allowance (ADA) as described in SSPC Guide 6 (not an average daily allowance) for evaluating the TSP monitoring results. The CIH  or CSP, or a person working under the direction of the CIH/CSP, shall provide a written report and analysis of monitoring results, including the relevant acceptance criteria based on the ADA, within five days of sample collection.  Provide a copy of the results to the Engineer the following work day after receipt.

DELETE:	436.03.35 Field Cleaning Waste Disposal, in its entirety.

INSERT:	The following.

436.03.35 Field Cleaning Waste Disposal.  Store all project waste, regardless of whether or not toxic metals may be present, in sealed 55-gallon drums. Drums shall be labeled with the structure number, Contract number, Contractor’s name, contents, and the date. Refer to 436.03.36 through 436.03.41.

When the waste is hazardous, comply with SSPC Guide 7. Each day, collect clothing and other waste material and seal them in 55-gallon drums. The drums shall be sealed 55-gallon open head type drums meeting I.C.C. Specification 17-H. All drums shall be in new condition.

DELETE:  The first paragraph in 436.03.37.  “When the project…random and representative.”

INSERT:  The following.

436.03.37 Waste Sampling and Analysis.  When the project involves hazardous waste, the CIH or CSP, or an employee working under the direct supervision of the CIH or CSP, shall take at least four samples of the accumulated residues of each waste stream collected at each structure or a sample from every third drum, whichever is greater. All sampling shall be random and representative.