CATEGORY 900

MATERIALS

SECTION 915 — PRODUCTION PLANTS

915.02 ASPHALT PLANTS

DELETE:  The second sentence in 915.02 (f)(2).

915.02.03 Responsibilities of the Administration.

DELETE:  Dispute Resolution in its entirety.

INSERT:  The following.

Dispute Resolution.  Following is the procedure to resolve conflicts resulting from discrepancies between test results from the Office of Materials Technology’s (OMT) Asphalt Technology Division or their designated AASHTO accredited third-party testing laboratory and the producer.

Verification. The producer and/or Project Engineer will provide a written dispute to OMT’S ATD Chief describing the nature of the dispute along with any pertinent information. Also provide OMT’s Deputy Director for Material Quality with a copy of the written dispute.

The written dispute must be filed within five business days after receiving QA data from OMT. If the dispute was filed by the producer only, then OMT will inform the Project Engineer. The dispute will only be considered for review if test results are outside the multi-lab or operating tolerance limits for any particular test of concern.

ATD’s Assistant Division Chiefs will review the pertinent information and report to the Chief. The Chief will report the findings of their review to the producer. This process will take three business days from the day written notification was received. This level will identify if further investigation or retesting is required.

Check Testing.  Check testing will be performed on a split sample from the next day’s production by the producer and OMT’s Central Laboratory to determine any sampling/testing errors. The Producer and/or OMT can witness the testing performed by each laboratory if requested.

Verification and Check Testing will be completed within three to five business days from the day of the agreement and will focus on the questionable test results. If the issue is still not resolved, refer to Third-party Testing.

Third-party Testing.  The producer and OMT will employ an AASHTO accredited laboratory to perform testing using split of the original sample. The lab whose test results vary the most from the test performed by the third-party lab will pay for the testing. The new test results will replace the original test results in the pay factor calculations. Third-party results will be considered binding unless the dispute is resolved without third-party testing, then mutually agreed upon test results will be considered binding. Testing shall be completed by the third-party testing laboratory within ten (10) business days of sample receipt.

Dispute Resolution Process for Discrepancies Related to Non-Test Results:  The resolution process for non-test related disputes (pay factor calculations, turnaround times or mix design approvals) of sufficient magnitude to impact payment is as follows:

- When a non-test related dispute arises, the producer or Project Engineer will file a written dispute with the ATD Chief describing the nature of the dispute along with the pertinent information. The OMT Deputy Director of Material Quality will be copied on all written disputes. The written dispute must be filed within five business days from when the issue arises.

- The ATD Chief or Deputy Director of Material Quality will appoint a panel of three members to provide recommendations to resolve the dispute.  The panel will include a member selected by the asphalt industry.

- The panel will make recommendations to the ATD Chief within five business days from the appointment.

- The ATD Chief or Deputy Director of Material Quality will decide the disposition of the dispute based on the panel’s recommendations.

- A written report from the panel describing all subsequent actions and final disposition of the dispute shall be included in the project records.

- The process will be completed within ten business days from the date of notification. If subsequent disputes arise on the same issue, the written report will be included as a resource during the resolution process.

DELETE:  SECTION - 915.03 PORTLAND CEMENT CONCRETE PLANTS in its                                    entirety.

INSERT:  The following.

915.03  PORTLAND CEMENT CONCRETE PLANTS. M 157, except as modified herein, including the applicable requirements of 915.01

915.03.01 Aggregate Storage. All aggregate used in portland cement concrete shall be maintained at a uniform moisture content in excess of its saturated surface dry condition. Water used shall meet 921.01.

915.03.02 Moisture Probes.  Moisture probes may be used in place of actual daily moisture testing of fine aggregate. Calibrate and maintain moisture probes per the manufacturer’s recommendations.

- Perform actual moisture tests for fine aggregate weekly and as directed. When the actual tests of the fine aggregate indicate a difference of greater than 0.5 percent free moisture than the moisture probe readings, immediately perform a second actual test.

- If the second test indicates a moisture difference of greater than 0.5 percent, recalibrate the moisture probe and verify. Records of all calibrations and weekly tests shall be maintained and made available.

915.03.03 Mixing Temperatures. The plant shall be equipped with approved methods of heating and cooling the mix. The temperature of the plastic concrete shall meet 902.10.03. The temperature of the cementitious materials and water during mixing shall not exceed 170 F.

915.03.04 Load Tickets. M 157.  Provide an approved computer generated batch ticket indicating the pertinent information for each load in duplicate. The ticket shall indicate maximum allowable water and maximum water allowed for jobsite slump adjustment.

Distribute load tickets as specified in 915.03.06 (c)(2). The producer’s copy shall be readily available for inspection upon request.  Issue a Form 116 for each load in the event a computer generated batch ticket cannot be provided.

915.03.05 Mixers and Agitators. M 157 except as follows.

- Operate drums during transit at agitating speed only.  Mixing during transit is prohibited.

- Add at least 85 percent of design water requirement at the plant through the certified plant water meter.

- Water for slump adjustment may be added at the plant through truck water system under the supervision of the certified concrete technician, provided the maximum specified water/cement ratio is not exceeded.

- A maximum of 3 gal of water per cubic yard of concrete may be added at the point of discharge provided it does not exceed the maximum specified water/cement ratio.

- No water may be added after partial discharge of the load.

- Loading of mixers or agitators that contain wash water in the drum is prohibited.

- When the concrete is specified or permitted to be produced by volumetric batching and continuous mixing, the batching and mixing unit shall meet C 685. Calibration shall meet MSMT 558.

- The minimum mixing time is 75 seconds for stationary mixers not subject to mixer performance tests.

915.03.06 Certified Concrete Plant. The producer shall be responsible for quality control of plant operations to ensure that the material meets as specified. The quality control process will be subject to unannounced periodic inspection by representatives of the Concrete Technology Division (CTD). Full participation in the inspection by the plant’s certified technician is required.

Initial and Annual Inspection. Any plant initially setting up and annually thereafter will be subject to a comprehensive inspection to determine whether the plant equipment and personnel meet all applicable requirements. The Administration will accept certification that the plant facilities meet all applicable requirements from either of the following:

- National Ready Mixed Concrete Association (NRMCA) Plant Certification Program. The Administration will review NRMCA Plant Certification Data and annually issue a written Plant Certification Approval.  The Administration will perform QA visits as needed to validate the plant certification.

- A Professional Engineer registered in the State of Maryland with at least 5 years operational or technical experience in concrete production. The Administration will review the Engineer’s inspection report and issue a written Plant Certification Approval.

- The Administration will conduct the inspections only if (a) and (b) are not feasible or applicable. The cost for inspection will be charged to a current Contract if applicable or to the ready mix producer if a current Contract is unavailable.

Responsibilities of the Concrete Producer.

- Notification. Notify CTD one working day prior to producing materials for Administration projects. Notify CTD at least five working days in advance of scheduling   the comprehensive inspection.

- Quality Control. Have the certified concrete plant technician present while concrete is being batched and delivered to Administration projects. This technician shall supervise concrete production.

- Develop and use an acceptable Quality Control Plan (QCP) that addresses all elements necessary for plant quality control. Submit the QCP for review and approval at the time of the annual comprehensive inspection. The QCP shall include the names, qualifications and responsibilities of a Quality Control Manager and Quality Control Technicians.

- Control tests shall be performed by or under the direct supervision of the certified concrete plant technician. The technician shall perform moisture tests, adjust proportions of aggregate for free moisture, complete and sign batch or approved delivery tickets, and ensure quality control of the batching operations.

- Concrete Plant Technician certification will be awarded upon satisfactory completion of examinations administered by the Administration.

- Supply all necessary test equipment.

- Sampling and testing shall meet the procedures and frequencies outlined in the Material Quality Assurances Processes, Details and Frequencies manual.

- Reports. The following reports shall be processed by the producer.

- Administration Form 113, daily. Provide a copy for the producer’s plant file for review.

- Load Tickets for each load. Provide a copy for the project and producer’s file.

- Administration forms for all concrete materials sampled at the plant.

- Test Worksheets for all tests performed daily at the plant.

- Provide a Monthly Production Report to CTD via e-mail to concrete@sha.state.md.us by the 10th of each month.  Report the total cubic yards and the total weight of each type of supplementary cementitious material used in concrete production for Administration projects for the previous calendar month.

- Inspectors Office. The producer shall provide an onsite office meeting the basic 
requirements of Section 103 Type A - Engineers Office for the exclusive use of SHA Engineers and Inspectors, as approved by the Engineer. The requirement for a mobile office trailer is waived.

Responsibilities of the Administration.

- Comprehensive Inspection and Acceptance Inspection and Testing.

  - The Quality Control Manager will be notified immediately to correct any deficiencies found during an Administration inspection to the satisfaction of the Engineer.  Production will be suspended for deficiencies where the quality of the product is affected, as determined by the Administration.

  - If critical deficiencies are found or consecutive inspections reveal identical or additional deficiencies, a Non-Compliance Report (NCR) will be issued to the Quality Control Manager detailing the findings and actions to be taken by the producer.

  - The Administration reserves the right to assign an Inspector to monitor operations for a maximum of five Administration production days. If at the end of this period the quality control process is not satisfactory, a NCR will be issued and plant approval will be rescinded. The plant shall be recertified before Administration production can continue.

- Recertification of Concrete Plant. Documentation of corrective action shall be submitted to the CTD by a professional engineer registered in the State of Maryland.  A comprehensive inspection will be conducted by the Administration to recertify the concrete plant once the documentation is approved.

- Independent Assurance Audits (IAA).  The Administration will evaluate the equipment and the proficiency of QC technicians through audits performed on a random basis.  The QC technician shall cooperate with the IAA technician in the evaluations.

- Technician Certification.  Conducted per the Mid-Atlantic Region Certification Program (MARTCP) and the Maryland Technician Certification Program.

DELETE:	SECTION - 915.05 CERTIFIED PRECAST CONCRETE PLANTS in its 
                        entirety.

INSERT:	The following.

915.05  CERTIFIED PRECAST CONCRETE PLANTS  Shall meet the applicable requirements of  915.01, 915.03 and the following.

Certified Precast Concrete Plant. The producer shall be responsible for quality control of plant operations to ensure that the material meets specification requirements. The quality control process will be subject to unannounced periodic inspection by representatives of the Concrete Technology Division (CTD). Full participation in the inspection by the plant’s certified technician will be required.

All plants producing precast concrete items of any description for Administration contracts shall be certified as appropriate by one or more of the following at the time of their Annual Inspection:

- The American Concrete Pipe Association (ACPA)

- The National Precast Concrete Association (NPCA)

- The Precast/Prestressed Concrete Institute (PCI).

Plants may be required to hold multiple certifications in order to produce a variety of products.

Initial and Annual Inspection.   The Administration will perform comprehensive initial and annual inspections on all plants to ensure that the plant equipment and personnel meets all applicable specification requirements.  The Administration will accept certification that the plant facilities meet all applicable requirements from a professional engineer registered in the State of Maryland with at least 5 years operational or technical experience in concrete production. Final acceptance and approval will be as determined by the Administration.

The cost for inspection will be charged to a current Contract if applicable or to the precast producer if a current Contract is unavailable.

915.05.01  Responsibilities of the Precast Concrete Producer.

- Notification. Notify CTD 14 days prior to producing any precast items for each Administration project. Notify CTD at least five working days in advance of scheduling   the comprehensive inspection.

- Quality Control. Have the certified quality control technician present while concrete is being batched and cast. The technician shall supervise all aspects of precast concrete production.

- Quality Control Procedures.  Quality control procedures shall be detailed in the Quality Control Plan and include the following:

- The method of inspecting reinforcement steel placement and forms prior to pouring concrete.

- The method of curing the concrete.

- The method of maintaining accurate quality control records.

- Samples of documents approved by the Engineer.

- Patching procedures.

- Methods of preparing the concrete units for shipment.

- A method of identifying each piece as tested and approved by quality control.

- When required, the producer shall submit a repair procedure for the precast product for approval that conforms to PCI Manual 137 and all other applicable specifications. All materials used for repairs shall be supplied from approved sources.

- Develop and use an acceptable Quality Control Plan (QCP) that addresses all elements necessary for plant quality control. Submit the QCP for review and approval at the time of the annual comprehensive inspection. The QCP shall include the names, qualifications and responsibilities of a Quality Control Manager and Quality Control Technicians.

- All precast concrete products shall meet the Standards or approved working drawings.  All materials shall be from an Administration approved source and meet all applicable specifications.

- The plan shall indicate how the producer intends to handle all of its materials.

- Sample and testing frequency and certification of materials shall meet the Material Quality Assurances Processes, Details and Frequencies manual.

- The producer shall submit a repair procedure for approval conforming to PCI Manual 137 and all other applicable specifications.  All materials used for repairs shall be supplied from approved sources.

- Quality Control Technician. Certified Quality Control Technicians shall hold the following certifications:

- Maryland State Highway Administration – Office of Materials Technology Certified Concrete Plant Technician (Certified Plant Technician)

- American Concrete Institute (ACI) Level I

Technicians shall also hold one of the following certifications as required:

- PCI Level I,

- NPCA Production & Quality School (PQS) Level I,

- ACPA Q-Cast Certified Technician.

- Test Equipment and Facilities. Supply all necessary test equipment and provide Administration-approved facilities suitable for conducting the various tests required. Off-site test facilities shall be approved by the Engineer.

- Reports. The following reports shall be processed by the producer:

- Load Tickets for each load. Provide a copy for producer’s file for review.

- Administration Forms for all concrete materials sampled at the plant.

- Test Worksheets for all tests performed daily at the plant.

- Provide a Monthly Production Report to CTD via e-mail to concrete@sha.state.md.us by the 10th of each month.  Report the total cubic yards and the total weight of each type of supplementary cementitious material used in concrete production and the total number of precast items shipped to Administration projects for the previous calendar month.

- Inspectors Office. The producer shall provide an onsite office meeting the basic 
requirements of Section 103 Type A - Engineers Office for the exclusive use of SHA Engineers and Inspectors, as approved by the Engineer. The requirement for a mobile office trailer is waived.

915.05.02  Responsibilities of the Administration

- Comprehensive Inspection.

- Verification Testing.

- Verification of certification will be performed a minimum of once per year at the           Administration’s discretion.

- The Administration reserves the right to discontinue acceptance of precast units if verification indicates that materials or test procedures do not meet the Contract Documents.

- Acceptance Inspection and Testing.

  - If deficiencies are found during an Administration inspection, the Quality Control Manager will be notified immediately to correct the deficiencies to the satisfaction of the Engineer. Production will be suspended for critical deficiencies where the quality of the product is affected as determined by the Administration.

  - If critical deficiencies are found or consecutive inspections reveal identical or additional deficiencies, the Engineer will issue a Non-Compliance Report (NCR) to the Quality Control Manager detailing the findings and actions to be taken by the producer.

  - The Administration reserves the right to assign an Inspector to monitor plant operations for a maximum of five Administration production days. If at the end of this period the quality control process is not satisfactory, a NCR will be issued and plant approval will be rescinded. The plant shall be recertified before Administration production can continue.

- Recertification of Precast Concrete Plant.  Documentation of corrective action shall be submitted to the CTD by a Professional Engineer registered in the State of Maryland.  After approval of the corrective action documentation, a comprehensive inspection will be conducted to recertify the concrete plant.

- Independent Assurance Audits (IAA).  The Administration will evaluate the equipment and the QC technicians’ proficiency through audits performed on a random basis.  The QC technician shall cooperate with the IAA technician in the evaluations.

- Technician Certification.  Conducted per the Mid-Atlantic Region Technician Certification Program (MARTCP) and the Maryland Technician Certification Program.