Section-557 should be used in conjunction with this Specification.

CATEGORY 900

MATERIALS

SECTION 951  PAVEMENT MARKING MATERIALS

DELETE:  SECTION 951.07 – SNOWPLOWABLE RAISED PAVEMENT MARKERS (SRPM) AND RECESSED PAVEMENT MARKERS in its entirety.

INSERT:  The following.

951.07 SNOWPLOWABLE RAISED AND NON-SNOWPLOWABLE RAISED PAVEMENT MARKERS.  Snowplowable Raised Pavement Markers (SRPM) include markers installed in steel or polycarbonate holders or by direct application into a groove.  Non-Snowplowable Raised Markers (NSRPM) are used with temporary pavement markings.

951.07.01. Pavement Marker Reflector Lenses.  Pavement marker reflector lenses shall be 4.00 x 2.00 x 0.46 in.  The slope of the reflecting surface shall be 30 degrees and the area of each reflecting surface shall be 1.7 in.2 The outer surface of the shell shall be smooth except in identification areas.  All pavement marker reflector lens shall be imprinted with the manufacturer’s name and the model number.

- Lenses for SRPMs with Holders.  D 4383.  Pavement marker reflector lenses shall be comprised of materials with adequate chemical, water and UV resistance for the intended use capable of being installed in a steel casing or recessed polycarbonate holder and shall conform as specified.  The reflector lens shall contain one or two prismatic reflective faces to reflect incident light from opposite directions.  The reflector lens shall be in the shape of a shallow frustum of a pyramid.  The bottom of the reflector lens shall be equipped with either an elastomeric pad to permit its attachment to the surface of the holder or the manufacturer’s recommended adhesive may be used.  The surfaces of the lens faces shall provide extremely durable abrasion resistance. Holders for the markers shall be either a steel casting or a plastic holder that is recessed in a groove.

- Lenses for Direct SRPMs without Holders.   D 4383.  Pavement marker reflector lenses be comprised of materials with adequate chemical, water and UV resistance for the intended use and shall conform as specified. The reflector lens shall contain one or two prismatic reflective faces to reflect incident light from opposite directions.  The reflector lens shall be in the shape of a shallow frustum of a pyramid.  The housing for the lens shall be designed for application directly to the pavement in the specified groove

951.07.02 SRPM Adhesive.  M 237, Type IV.  Use to fasten the SRPM holders and Direct SRPMs to the pavement as specified. Rapid set adhesives shall not be used. The surface of all marker lenses shall be free of gloss or substances that will inhibit bonding of the adhesive.

951.07.03 SRPM Holders

- Steel Casting.  D4380.  A 536, Grade 80-55-06, hardened to 51 to 55 RC per E18.  Casting dimensions shall be a minimum of 9.25 x 5.86 x 1.69 in. and shall not exceed 10.5 x 7.25 x 1.69 in.  Steel holders shall be capable of holding the marker above the pavement. Both ends of the steel holder shall be shaped to deflect a snow plow blade.  The bottom of the steel holder shall incorporate two parallel keels and an accurately shaped web designed to fit into a grooved surface.  The installed height shall not exceed 0.25 in. above the road surface.

The surface of the keel and web shall be free of scale, dirt, oil, grease or any other substance that may reduce its bond to the epoxy adhesive.  The casting shall be imprinted with the manufacturer’s name and the model number.

- Polycarbonate.  A polycarbonate plastic material with dimensions of 5.00” x 3.00” x 0.70” capable of holding a SRPM lens recessed in a 1/8” groove below the pavement surface. The polycarbonate holder shall have tabs capable of extending out onto the pavement for the purpose of proper positioning.  The surface of the housing shall be free of dirt, oil, grease or any other substance that may reduce its bond to the epoxy adhesive.

951.07.04 Reflector Lens Adhesive.  Used to fasten the reflector lens to the holder in accordance with the manufacturer’s recommendations.

951.07.05 Non Snowplowable Raised Markers.  D 4280.  NSRPMs. shall be comprised of materials with adequate chemical, water and UV resistance for the intended use and shall conform as specified.  The reflector lens shall contain one or two prismatic reflective faces to reflect incident light from opposite directions.  The reflector lens shall be in the shape of a shallow frustum of a pyramid.  The bottom of the reflector lens shall be equipped with either a pressure-sensitive elastomeric pad to permit its attachment to the surface or be capable of being installed using a hot bitumen adhesive per the manufacturer’s recommendations.

951.07.06 Field Evaluation.  SRPMs shall be evaluated on the National Transportation Product Evaluation Program’s (NTPEP) North Test Deck.  NSRPMs may be field evaluated on any NTPEP Test Deck.  SRPMs and NSRPMs that perform satisfactorily throughout the evaluation period will be placed on the Administration’s Qualified Products List (QPL).  Random testing of samples will be performed and conformance will be determined by the Office of Materials Technology (OMT).

951.07.07 Quality Assurance Sampling.  Refer to 549.03.02.

951.07.08 Material Shipment.  SRPMs and NSRPMs shall be shipped in containers sealed by the manufacturer.  The label on each container shall include the following.

- Manufacturer’s Name.

- Place of Manufacture.

- Color of Material and Component Type.

- Date of Manufacture (month-year).

- Batch and Lot Identification Number.

- Size/quantity of lot represented.

951.07.09 Certification.  Furnish certification for all SRPMs and NSRPMs per TC-1.03.  All SRPMs and NSRPMs supplied shall conform to the identical composition of the samples submitted for NTPEP evaluation.  Identify SRPMs and NSRPMs by referring to the code used on the test deck SRPMs and NSRPMs that fail to conform will be rejected.

The manufacturer shall also provide the following.

(a)	Material Safety Data Sheets for all materials submitted for testing and use.

- A facility capable of producing the SRPMs and RPMs in the quantity and quality required.

(c)	A laboratory capable of performing the required tests; subject to Administration approval.