Category 300

Drainage

SECTION 316 — Stormwater Management (SWM) Filtration Facilities

316.02 MATERIALS

DELETE:  The paragraph of “Subdrain Pipe, Fittings and Geotextile Sock.  Perforated and solid-wall… manufacturer.”

INSERT:  The following.

316.02.01 Subdrain Pipe, Fittings, and Geotextile Sock.  Subdrain pipe shall include slotted perforated and solid-wall (non-perforated) pipe.  Perforated subdrain pipe shall have only two rows of perforations.  Use fittings matching the same material as the subdrain pipe and is otherwise compatible with the subdrain pipe.  Use subdrain pipe, fittings, and geotextile sock for subdrain, cleanouts, and observation wells.

- Subdrain Pipe. Pipe material for perforated subdrain pipe may be one of the following.

  - Polyvinyl chloride (PVC) profile wall drain pipe (PPWP) with soiltight joints, slotted perforations not to exceed 0.12 in. in width with a minimum water inlet area of 1 in.2/ft (for pipe diameters 6 in. to 10 in.) or 1.5 in.2/ft (for 12 in. diameters), and meeting M 304.

  - Corrugated polyethylene drainage pipe (CPP) Type SP with Class 2 slotted perforations having a minimum water inlet area of 1 in.2/ft (for pipe diameters 3 in. to 10 in.), and meeting M 252.

- Subdrain Pipe Cleanouts. Pipe material for non-perforated or solid wall subdrain pipe used for cleanouts may be one of the following and compatible with the subdrain pipe used in 316.02.01(a).

  - Polyvinyl chloride (PVC) profile wall drain pipe (PPWP) with soiltight joints and meeting M 304.

  - Corrugated polyethylene drainage pipe (CPP) Type S and meeting M 252.

- Observation Wells. Pipe material used for observation wells shall be as specified in 316.02.01(a) for the perforated portion of observation wells and 316.02.01(b) for the solid-wall portion of observation wells.  Use the geotextile sock recommended and supplied by the subdrain pipe manufacturer and use only to cover the perforated pipe portion of observation wells.