CATEGORY 900

MATERIALS

SECTION 911 — Joints

DELETE:  911.01 JOINT SEALER AND CRACK FILLER in its entirety.

INSERT:  The following.

911.01 JOINT SEALER AND CRACK SEALER.  Sealant material shall meet the requirements of classification Type II according to D6690 as modified by MSMT 404.  The manufacturer shall furnish certification as specified in TC-1.03.  Manufacturer’s recommendations regarding heating and pouring temperatures will be used when testing these materials.  If a range of temperatures is recommended, the midpoint will be used as the pour point.

911.01.01 Silicone Joint Sealer and Crack Sealer. Low modulus, one component compounds.  If a primer is required, it shall be as recommended by the sealant manufacturer and be placed on the joint faces following the insertion of the backup material.

Silicone material, when tested at 73 ± 3 F and 45 percent to 55 percent relative humidity, shall meet the following:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Shore A Hardness, at 7 days | D2240 | 10-25 |
| Tensile Strength at 150 % Elongation, psi max | D412 Die C | 45 |
| Elongation, % min | D412 Die C | 700 |
| Adhesion in Peel, lb/in. min | Fed Spec TT-S-00230 | 20 |
| Flow, 0.01 in. max | T 187 | 0.3 |
| Tack-Free Time, minutes | D2377 | 20-75 |

Each container of silicone sealer and crack sealer shall have a shelf life of at least six months. Material more than six months old shall be retested.