Category 900

MATERIALS

SECTION 915 — Production Plants

915.04 BASE COURSE PLANTS

DELETE:  915.04.01 Nonstabilized in its entirety.

INSERT:  The following.

915.04.01 Non-Stabilized. Base course plants producing graded aggregate base material without a stabilizing agent shall meet 915.01 and the following:

- Produce the material in a processing plant using qualified aggregate sources and approved job mix formula.

- Submit the Quality Control Plan to the Soils and Aggregate Technology Division (SATD) of OMT for approval prior to production.

- The production shall meet the gradation requirements of the approved job mix formula.

- Maintain the required moisture content according to the approved job mix formula prior to shipment.

- Maintain stockpiles to prevent segregation.

- Frozen aggregates shall not be used.

- Mixed material shall be handled and transported in a manner that will minimize segregation and the loss of moisture.  All loads shall be covered with suitable material of sufficient size to completely protect it from the weather and in accordance with State laws.

DELETE:  915.04.02 Stabilized in its entirety.

INSERT:  The following.

915.04.02 Stabilized.

- Mechanical mixers shall be used, as approved.  All plants shall be equipped with automatic cutoff devices interlocked so the plant will stop operating if delivery of any component of the mix fails.

- The amount of stabilization shall be measured according to MSMT 254.

- The charge in a batch mixer or rate of feed to a continuous mixer shall not exceed the capacity that will permit complete mixing of all materials.

- Mixed material shall be handled and transported in a manner that will minimize segregation and the loss of moisture.  All loads shall be covered with suitable material of sufficient size to completely protect it from the weather and in accordance with State laws.

- The required moisture content shall be maintained according to the approved job mix formula prior to shipment.

- When emulsified asphalt is used as a stabilizing agent, all aggregate shall contain moisture in excess of the saturated surface dry condition at time of mixing.

DELETE:  915.04.03 Certification of Base Course Plants in its entirety.

INSERT:  The following.

915.04.03 Certification of Base Course Plants. The quality control and condition of all materials used in base courses, as well as all necessary adjustments required in using the materials, is the responsibility of the base course producer.  The quality assurance process will be subject to unannounced periodic inspection by representatives of the SATD when Administration projects are in progress.  The plant’s certified technician shall participate in the inspection.

915.04.03.01 Initial and Annual Inspections. Any plant initially setting up and annually thereafter will be subject to a comprehensive inspection to determine whether the plant equipment and personnel meet all applicable requirements.  After the initial inspection, the plant shall meet 915.01.04.

- The Administration can conduct the initial or annual inspection.  The cost for inspection will be charged to a current Contract if applicable or to the base course producer if a current Contract is unavailable.

- The Administration will accept certification by a professional engineer registered in the State of Maryland with at least five years operational or technical experience in base course production.  The Administration will review the Engineer’s inspection report and issue a written Plant Certification Approval.  Final acceptance will be determined by the Administration.

915.04.03.02 Responsibilities of the Base Course Producer.

- Notification. Notify SATD one day prior to producing materials for Administration projects.  Report total tons shipped one business day after completed daily shipments.  Send report to gab@mdot.maryland.gov.

- Quality Control. The producer is responsible for quality control of plant operations to ensure that the material meets specification requirements.  All producers supplying base courses shall have a certified base course Plant Technician present while base course material is being plant mixed and delivered to the project.  The Plant Technician shall perform quality control sampling, testing, and documentation as specified.

  - Control tests shall be performed by a certified base course plant technician.  This technician shall obtain samples and test according to the current version of the Material Quality Assurance Process Manual for Soils and Aggregate Technology Division, Aggregate Materials, Controlled Mixtures.

  - Technician certification will be awarded upon satisfactory completion of a written and practical examination given by the Administration.

  - Supply all necessary test equipment and provide on-site facilities suitable for conducting the required tests.

- Reports.

  - Prepare and submit the following reports to SATD at gab@mdot.maryland.gov:

    - MDOT SHA Form 43, daily, stating that the material was sampled and tested using the Administration’s sampling and testing guidelines and meets the applicable specifications.

    - MDOT SHA Form 88, for all additives introduced at the plant.

  - Producer shall keep a record of the following forms at the Plant:

- Daily Plant Certification Form (MDOT SHA Form GA-1) showing that a technician was on duty at the plant.

- The Producer’s Daily Quality Control test worksheet, for all tests performed at the plant.

- Base Course Plant Daily Production log sheet posted on the GAB Bulletin Board.

915.04.03.03 Responsibilities of the Administration.

- Comprehensive Inspection – SATD/OMT will perform the Initial or Annual inspection.

- Quality Assurance Inspection and Testing – Will be performed according to the current version of the Material Quality Assurance Process Manual for SATD, Aggregate Materials, Controlled Mixtures.

  - If deficiencies are found, as defined in the base course plant checklist during a quality assurance inspection, the producer will be notified immediately, and operations will be suspended if corrections are not made to the satisfaction of the Engineer.

  - If consecutive inspections reveal identical or additional deficiencies, a Non-Compliance Report (NCR) will be issued to the Quality Control Manager detailing the findings and actions to be taken by the producer.

  - A reinspection will be held in two Administration production days.  All deficiencies shall be corrected by the reinspection date.  OMT will determine whether plant certification will be revoked.

- Independent Assurance Audits (IAA). The Administration will evaluate the equipment and the proficiency of QC technicians through audits performed on a random basis.  The QC technician shall cooperate with the IAA technician in the evaluations.

- Recertification of Aggregate Base Course Plant. Documentation of corrective action shall be submitted by a Professional Engineer registered in the State of Maryland with at least five years operational or technical experience in base course production.  When this documentation is approved, a comprehensive inspection will be conducted to recertify the base course plant.

- Technician Certification. Conducted according to the Mid-Atlantic Region Technician Certification Program (MARTCP) and the Maryland Technician Certification Program.