Category 900

Materials

SECTION 917 — Miscellaneous Protective Coatings

DELETE:  917.03 FUSION BONDED POLYESTER POWDER in its entirety.

INSERT:  The following.

917.03 FUSION BONDED POLYESTER POWDER SYSTEM

917.03.01 Materials. The polyester powder system shall consist of an epoxy zinc rich primer and a super durable TGIC (Triglycidyl Isocyanurate) polyester topcoat.  The finish powder shall be a TGIC polyester powder.  The polyester powder manufacturer shall be selected from the QPL maintained by OMT.

# 917.03.02 Primer. Primer shall be an epoxy zinc rich primer supplied by the same manufacturer as the finish powder.  Primer shall meet the following:

| # TEST PROPERTY | # TEST METHOD | # SPECIFICATION LIMITS |
| --- | --- | --- |
| # Salt Spray 3000 hrs | # B117 | # < 1/32 in. undercut, no blisters |
| # Humidity resistance # 3000 hrs | # D2247 | # < 1/32 in. undercut, no blisters |
| # Hardness | # D3363 | # 2H-3H |
| # Adhesion | # D3359 | # 5B |

917.03.03 Qualification Requirements. The following physical tests will be required to qualify the polyester and are not required for certification.

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Abrasion Resistance | D1044 - Taber Abraser CS-10, 1000 gm load, 1000 cycles, | 100 mg max weight loss |
| Adhesion | D3359, Method A (Bonderite 1000 panel) | Rating 5A |
| Gloss | D525, 60° initial | 30 - 45 per AMS-STD-595A |
| Hardness | D3363 | Min 2H - No gouge |
| Impact | D2794 | Pass 80 in. lb |
| Salt Spray Resistance | B117, D1654 1000 hr (Bonderite 1000 panel) | Table 2, Rating 7 |
| Thickness | G12 | 7 ± 2 mills |
| Color | E1331 or E1338 | As specified in the Contract Documents from AMS-STD-595A Color No. 20040 |
| Infrared Spectrogram | Equipment manufacture's procedures | Manufacturer's IR |
| Weather Resistance | D4587, test condition D. Test shall be conducted with a UVA lamp (340 nm peak) for 1000 hr | 50% min gloss retention |
| Specific Gravity | D5965 | Manufacturer's result |
| Chloride Permeability | A775, A 1.3.4 | <0.000lM |

917.03.04 Certification. The polyester powder manufacturer shall furnish production batch certification as specified in TC-1.03 showing conformance to the following:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Infrared Spectrogram | D2621 | Match Qualification sample |
| Taber Abrasion Resistance, mg loss, max | 4060 | 100 |
| Specific gravity | D5965 (Method A) | Qualification sample ± 0.02 |
| Color | E1331 or E1338 | Match AMS-STD-595A color no. specified in Contract Documents |

917.03.05 Coating System.

| Powder | Coat | Dry Film Thickness | Usage |
| --- | --- | --- | --- |
| Epoxy primer | I | 2.5-4.0 | Primer |
| Polyester Powder | II | 5.0-7.0 | Finish |

917.03.06 Acceptance. Acceptance will be based on the quality control test results required on the manufacturer's certification.  The coating applicator shall be responsible for reviewing certifications to ensure conformance to TC-l .03.  The coating applicator shall also maintain a file of all reviewed certifications.