Category 900

Materials

SECTION 951 — Pavement Marking Materials

951.07 SNOWPLOWABLE RAISED AND NON-SNOWPLOWABLE RAISED PAVEMENT MARKERS

DELETE:  951.07.03 SRPM Holders in its entirety.

INSERT:  The following.

951.07.03 SRPM Holders

- Polycarbonate. A polycarbonate plastic material with dimensions of 5.00 in. x 3.00 in. x 0.70 in. capable of holding a SRPM lens recessed in a 1/8 in. groove below the pavement surface.  The polycarbonate holder shall have tabs capable of extending out onto the pavement for the purpose of proper positioning.  The surface of the housing shall be free of dirt, oil, grease, or any other substance that may reduce its bond to the epoxy adhesive.