CATEGORY 600

SHOULDERS

SECTION 602 — Curb, Combination Curb and Gutter, and Monolithic Median

602.02 MATERIALS

ADD:  The following as the first sentence.

Refer to 701.02, 705.02, 708.02, and the following:

DELETE:	  Portland Cement Concrete from the materials table.

INSERT:  The following into the materials table.

| Portland Cement Concrete | 902.10, Mix No. 13 |
| --- | --- |
| Common Borrow | 916.01 |
| Topsoil | 920.01.01, 920.01.02 |
| Subsoil | 920.01.03, 920.01.04 |

602.03 CONSTRUCTION

602.03.01 Concrete Curb, Combination Curb and Gutter, and Monolithic Median.

DELETE:  (f) Finishing in its entirety.

INSERT:  The following.

(f) Finishing.  Strike off the concrete to the specified cross section.  Finish, float, and apply a broom finish.  For matching adjacent concrete surfaces, other methods of finishing may be permitted.  Do not use plastering.  Use a 1 in. radius edging tool on the face edge of the curb.  Finish all other exposed edges with a 1/4 in. edging tool.  Limit any deviation from grade and alignment of the face and top surface of curbs and medians to no more than 1/4 in. in 10 ft.  Do not add water to the concrete at any time during any phase of the finishing operations.  Immediately after removal of the forms, repair all honeycombed and damaged areas.  Ensure an ACI Concrete Flatwork Finisher or NRMCA Concrete Exterior Flatwork Finisher is present at all times during finishing operations.

DELETE:	  (h) Cold Weather Construction and Curing in its entirety.

INSERT:  The following.

(h) Cold Weather Construction and Curing.  Refer to 520.03.02 and 520.03.12(a) White Pigmented, except the requirement for an approved spraying machine with drive wheels is waived.  Apply by sprayers in two directions at 90 degrees to each other, at a rate recommended by the manufacturer, completely covering the surface of the concrete.  Have standby equipment on site in the event of spraying equipment failure.  Do not allow pedestrian and vehicular traffic during the curing period.

DELETE:  (i) Backfill in its entirety.

INSERT:  The following.

(i) Backfill.  Backfill as directed.

(1) Non-Landscaped Areas.  Backfill with approved materials as specified in 204 or 701 to the grade that is 4 in. below the final grade.  Complete the backfill to the final grade with aggregate as specified or as directed.

(2) Landscaped Areas.  Backfill with topsoil up to 8 in. depth as specified in Section 701 and perform sodding or seeding as described in (3) below.  For backfill more than 8 in. depth, the use of aggregate fill is prohibited.  Install subsoil or approved common borrow as specified in Section 204 or Section 701 to the grade that is 4 in. below the final grade.  Complete the adjustment with topsoil as specified in Section 701 and perform sodding or seeding as described in (3) below.

(3) Sodding or Seeding.  Immediately after placing topsoil, perform Turfgrass Sod Establishment as specified in Section 708.  Alternatively, perform Turfgrass Establishment as specified in Section 705 and install Type A or Type E Soil Stabilization Matting as specified in Section 709.

602.03.02 Asphalt Curb.

DELETE:  The third paragraph in its entirety, “When required…or rolling.”

INSERT:  The following.

When required, backfill the curb as specified in 602.03.01(i) after the asphalt curb has sufficiently hardened to prevent damage.

602.04 MEASUREMENT AND PAYMENT

DELETE:  The first sentence of the second paragraph, “The removal and disposal…replacement material.”

INSERT:  The following.

The removal and disposal of unsuitable material will be measured and paid for at the Contract unit price for Class-1A Excavation, which price includes the cost of using acceptable excavation as replacement material.

DELETE:  The third paragraph in its entirety, “When existing curb…new item.

INSERT:  The following.

When existing curb, combination curb and gutter, or monolithic median are removed and replaced with new curb, combination curb and gutter, or monolithic median, the cost of the removal will be paid for as specified in 206.04.02.