CATEGORY 600

SHOULDERS

SECTION 603 — Sidewalks

603.02 MATERIALS

ADD:  The following as the first sentence.

Refer to 701.02, 705.02, 708.02, and the following:

DELETE:	  Portland Cement Concrete from the materials table.

INSERT:  The following into the materials table.

| Portland Cement Concrete | 902.10, Mix No, 13 |
| --- | --- |
| Common Borrow | 916.01 |
| Topsoil | 920.01.01, 920.01.02 |
| Subsoil | 920.01.03, 920.01.04 |

603.03 CONSTRUCTION

603.03.01 Concrete Sidewalks

DELETE:	  (d) Finishing in its entirety.

INSERT:  The following.

(d) Finishing. Immediately after screeding and before bleed water appears, bull float the concrete to seat the coarse aggregate particles.  After bull floating and waiting until bleed water has dissipated and the concrete has begun to set, float the concrete to provide a level surface and apply a broom finish.  Do not plaster the surface.  Use a 1/4 in. edging tool on all outside edges and all joints.  On dry and/or windy days and as directed, while waiting for the concrete to set, apply a thin film of evaporation retarder according to the manufacturer’s recommendations.  Do not use evaporation retarder as a finishing aid.  Do not add water to the concrete at any time during any phase of the finishing operations.  Immediately following texturing and edging, begin the concrete curing.  Ensure an ACI Concrete Flatwork Finisher or NRMCA Concrete Exterior Flatwork Finisher is present at all times during finishing operations.

DELETE:  (f) Cold Weather Construction and Curing in its entirety.

INSERT:  The following.

(f) Cold Weather Construction and Curing. Refer to 602.03.01(h).

603.03.02 Asphalt Sidewalks.

DELETE:  (b) Placement and (c) Compaction in their entirety.

INSERT:  The following.

(b) Placement. Place asphalt mix as specified in 504.03.06.

(c) Compaction. Use an approved roller.  In areas inaccessible to a roller, a vibrating plate compactor or hand tamping may be used.  Compact the asphalt mix uniformly, starting compaction as soon as the asphalt mix can be compacted without displacement.  Continue until the material is thoroughly compacted and all marks have been removed.

603.03.03 Backfill

DELETE:  603.03.03 Backfill in its entirety.

INSERT:  The following.

603.03.03 Backfill.  Backfill as specified in 602.03.01(i).

603.04 MEASUREMENT AND PAYMENT

DELETE:  The first sentence of the second paragraph, “The removal and disposal…replacement material.”

INSERT:  The following.

The removal and disposal of unsuitable material will be measured and paid for at the Contract unit price for Class-1A Excavation, which price includes the cost of using acceptable excavation as replacement material.

DELETE:  The third paragraph in its entirety, “When the existing sidewalk…for sidewalk.”

INSERT:  The following.

When existing sidewalks are removed and replaced in the same location with new sidewalks, the removal will be measured and paid for as specified in 206.04.02.