Category 500

Paving

SECTION 504 — Asphalt Pavement

504.03 CONSTRUCTION

DELETE:  504.03.04 Tack Coat in its entirety.

INSERT:  The following.

504.03.04 Tack Coat.  Ensure the surface is dry and thoroughly cleaned by a power broom and/or air blowing prior to application.  Apply the tack coat by uniformly covering the entire surface to be paved using an application rate of 0.04 gal/yd2 to 0.10 gal/yd2 or as directed by the Contract documents.  Allow the tack coat time to thoroughly break and set.