Category 600

Shoulders

SECTION 604 — Concrete Traffic Barriers

604.02 MATERIALS

DELETE:

Portland Cement Concrete	902.10, Mix No. 6

Reinforcement Steel		Section 908

INSERT:  The following.

Portland Cement Concrete	902.10, Mix No. 6 or 420.02.04 and 902.10

Reinforcing Steel		Section 908, Grade 60, Epoxy Coated

Fusion Bonded Epoxy		917.02

DELETE: The first and second paragraphs in their entirety after the Materials table, “Use concrete mix No. 6…each source of supply.”

INSERT:  The following.

Use concrete mix No. 6 to construct all concrete traffic barriers, end transitions, and footers unless otherwise specified.

604.03 CONSTRUCTION

604.03.01 Concrete Barriers.

604.03.01 (b) Slip-form Method.

DELETE:  The fourth paragraph in its entirety, “Saw or form…or as directed.”

INSERT:  The following.

Saw or form construction and contraction joints at 20 ft intervals in the barrier and footer with a minimum of 10 ft, except in the area of miscellaneous structures 6 ft will be permitted.  Saw the joints 1/8 in. wide and at least 2 in. deep.  Use a diamond blade to saw cut contraction joints in the finished barrier.  Make cuts and space joints as specified.  Saw cut the contraction joints as soon as possible after initial concrete set and after the concrete has set sufficiently to preclude raveling during the sawing.  Complete the sawing the same day the concrete is extruded and before any shrinkage cracking occurs.  Do not leave concrete overnight without saw cutting the joints.  Place expansion joints as specified or as directed.  Terminate slip form placements at a barrier joint.