Category 900

Materials

SECTION 902 — Portland Cement Concrete and Related Products

902.03 HYDRAULIC CEMENT

DELETE: 902.03.02 Slag Cement in its entirety.

INSERT:  The following.

902.03.02 Slag Cement. M 302, Grade 100 or Grade 120.  The Contractor may request to substitute up to a maximum of 50 percent of the weight of Portland cement or Type IL Blended Hydraulic Cement with slag cement.  When slag cement is used, the minimum cement factor and water/cement ratio will be determined on the basis of the combined weight of the Portland cement or Type IL Blended Hydraulic Cement and slag cement.  Do not use slag cement and Type IP or Type IS Blended Hydraulic Cement in the same mix.

902.04 BLENDED HYDRAULIC CEMENT

DELETE: 902.04 BLENDED HYDRAULIC CEMENT in its entirety.

INSERT: The following.

902.04 BLENDED HYDRAULIC CEMENT. M 240 Type IP containing 15 percent to 25 percent Fly Ash by weight of blended cement, Type IS containing 25 percent to 50 percent slag cement by weight of blended cement or Type IL.  Maximum loss on ignition for Type IP or Type IS is 3.0 percent.  The requirement for a manufacturer’s written statement of the chemical composition is waived.

902.06 CONCRETE ADMIXTURES

902.06.04 Pozzolans.

DELETE:   The first paragraph “When a pozzolan is used…same mix.”

INSERT:  The following.

When a pozzolan is used, the minimum cement factor and water/cement ratio will be determined on the basis of the combined weight of the Portland cement or Type IL Blended Hydraulic Cement and pozzolan.  Do not use pozzolan and Type IP or Type IS Blended Hydraulic Cement in the same mix.

ADD:  The following after (b) Microsilica ...

(c) Natural Pozzolans.  M 295, pozzolan Class N, Natural Pozzolan may be substituted

up to a maximum of 30 percent of the weight of cement.

902.11 MORTAR FOR GROUT

DELETE:  The first sentence in its entirety, “Mortar used for…of the following:”

INSERT:  The following.

Mortar used for grouting reinforcement steel, anchor bolts, pipe, handrail posts, and miscellaneous items shall be composed in accordance with one of the following:

902.17 SELF CONSOLIDATION CONCRETE (SCC)

INSERT:  After the first paragraph of Note 2.

For e-ticketing, refer to 121.03.01.05 for all other required delivery ticket data requirements.