Category 300

Drainage

Access Road with cellular confinement load support system

DESCRIPTION

Construct access roads with cellular confinement load support systems.

MATERIALS

| No. 7 Aggregate | M 43, No. 7 |
| --- | --- |
| Geotextile, Non-Woven | 919.01, Class SE |
| Securing Pins and Staples | 919.03 |
| Topsoil | 920.01 |
| Fertilizer | 920.03.01 |
| Straw Mulch | 920.04.01 |
| Wood Cellulose Fiber | 920.04.02 |
| Soil Stabilization Matting (SSM) | 920.05, Type A |
| Fasteners for SSM | 920.05.02 |
| Seed | 920.06 |
| Turfgrass Sod | 920.06.03 |
| SHA Turfgrass Seed Mix | 920.06.07(a) |
| SHA Special Purpose Seed Mix | 920.06.07(b) |
| SHA Temporary Seed Mix | 920.06.07(c) |
| Water | 920.09.01 |

Geogrid.  Non-woven geotextile strips thermos-welded into a cellular system.  Cells shall be at least 2 in. long, 4 1/4 in. wide, and 2 in. deep.  When extended, the grid shall cover at least 107 ft2.

CONSTRUCTION

Prepare subgrade as specified in 208.03 and 211.03.02.

Place geotextile on the prepared surface for the full width of the area to be covered.  Unroll the geotextile parallel to the baseline.  Do not drag the geotextile across the grade.  Remove wrinkles and folds by stretching and pinning.  Overlap the end of 6the roll in the direction of aggregate placement.  Pin all roll ends and roll end overlaps a maximum of 5 ft on center.  Pin roll edges and roll edge overlaps a maximum of 5 ft on center.  For curves, fold or cut the geotextile and overlap in the direction of the turn.  Pin folds in the geotextile a maximum of 5 ft on center.  Immediately repair or replace damaged geotextile as directed.  Overlap geotextile patches at least 3 ft into undamaged geotextile.  Do not allow construction equipment on the bare geotextile.

Place aggregate on top of geotextile.  Use the end dumping and spreading method.  Place a single lift parallel to the baseline and at the thickness required to provide the specified compacted depth. Starting with a panel of geogrid, use temporary pegging to hold one end and pull the geogrid out to its maximum length of 26 ft.  This will reduce the width of the panel.  Do not overextend.  When necessary, cut the geogrid to shape or size.  Lay the next geogrid panel in the same way, adjacent to the first, and staple each of the open cell edges together to create a single panel out of the two grids.  Continue with this method of installing remaining panels of geogrid.  Exercise care and do not walk on the geogrid.  Walk only on timber boards placed on the geogrid when necessary to walk in areas of installed geogrid.  When on a slope, fix the grid at regular intervals on the ground with pegs.

Do not stand on the empty geogrid itself until completely filled.  Fill each end of the geogrid with a handful of aggregate to hold it in place.  Ensure the geogrid is in constant contact with the ground when placing aggregate into the geogrid cells.  Use a timber board on top of the geogrid to help better ensure contact is made.  Once the ends have been filled, remove the temporary pegs or push them completely into the ground for improved stability.  The geogrid may be filled manually or mechanically.  If filled mechanically, do not drop the aggregate from more than 18  in. above the ground.

Rake the aggregate into the geogrid cells so that they are filled to the top.  Once the area has been completed and the cells are filled to the top of the geogrid, place topsoil on the aggregate-filled geogrid cells as specified in 701.03.

Placement of Topsoil.  Place topsoil on the aggregate infill material to a minimum depth of 4 in. as specified in 701.03.

Perform Turfgrass Establishment as specified in Section 705 or Turfgrass Sod Establishment as specified in Section 708, whichever is applicable.  When turfgrass seed is applicable, also install Type A soil stabilization matting (SSM) as specified in Section 709.

MEASUREMENT AND PAYMENT

Access Road with Cellular Confinement Load Support System will be measured and paid for at the Contract unit price per square yard.  The payment will be full compensation for furnishing and installation of all geotextile, geogrid, aggregate, pegs, fasteners, pins, staples, and for all material, labor, equipment, tools, and incidentals necessary to complete the work.

Topsoil will be measured and paid for as specified in 701.04.

Soil Stabilization Matting (SSM) will be measured and paid for as specified in 709.04.

Turfgrass Establishment will be measured and paid for as specified in 705.04

Turfgrass Sod Establishment will be measured and paid for as specified in 708.04.

Replacement of damaged geotextile with undamaged geotextile will be at no additional cost to the Administration.