Category 400

Structures

SECTION 410 — Piling

410.03 CONSTRUCTION

410.03.06 Splicing.

DELETE:  the second and third paragraphs “When splicing of steel…piles less than 24 in. in diameter” in their entirety.

INSERT:  The following.

When splicing steel H piles and steel pipe piles is necessary, use electric arc welding conforming to the AWS Structural Welding Code for the full periphery and the welding criteria in AWS D1.1 for 24 in. or less diameter pipe piles or AWS D1.5 8.26 and Table 8.1 for over 24 in. diameter pipe piles and H piles.  The number of splices permitted shall be compatible with driving conditions at the site and the standard lengths of piling produced by manufacturers; however, only one section of each pile shall be less than 20 ft.

If the plans show separate steel pipe pile moment splice details that are to be used above a designated elevation, weld these splices as specified in 430.03 excluding the submerged arc welding requirement.  Field welders shall be qualified to 430.03.19(a).