Category 400

STRUCTURES

SECTION 426 — Latex Modified Concrete Overlay For Bridge Decks

426.03 CONSTRUCTION

426.03.03 Deck Removal and Repairs.

DELETE:  	The sixth paragraph in its entirety, “Existing reinforcing steel … Refer to 426.03.04 for additional requirements.”

INSERT:  The following.

Ensure that the existing concrete around the reinforcing bars is sound and not debonded especially when more than 1/2 diameter is exposed.  Where the bond between existing concrete and reinforcing steel has been destroyed, remove the concrete adjacent to the bar to a depth that will permit concrete bond to the entire periphery of the exposed bar.  Ensure that this clearance is at least 1 in. unless lower bar mats make it impractical.

Existing reinforcing steel utilized in the finished deck shall meet 421.03.07.  Take measures to prevent cutting, stretching, or damaging any exposed reinforcing steel. Regardless of whether it was previously coated, abrasive blast clean and apply epoxy coat touch up system to all exposed reinforcement as specified in Section 465.  Use epoxy powder coating touch up material from the Administration’s Approved List.  If the Contractor believes that there is not enough time to allow the system to properly cure, request a waiver for this requirement to the Office of Structures prior to the start of removal operations.  Replace the reinforcing steel that is damaged or deteriorated with the same diameter bars using epoxy coated bars for all existing reinforcing steel regardless of whether it was previously coated.  Refer to 426.03.04 for additional requirements.

DELETE:	  The eighth paragraph in its entirety, “Repair spalled concrete, voids … sufficient to meet this requirement”

INSERT:  The following.

Repair spalled concrete, voids, and other defects that are located within the proposed LMC overlay area according to the methods specified herein.  Each repair includes the removal of the additional deck material, all hand-chipping, and filling the repair area voids with LMC overlay while applying the overlay.

- For cavities less half the deck thickness, no additional work required.

- For cavities over half the deck thickness but not full depth, furnish and erect temporary protective shields as specified in 405.03.01.  If utilized in the original construction of the structure, existing stay in place forms that are in good condition will be sufficient to meet this requirement.

- For areas where the depth of removal is full depth, meet the following in addition to the requirements of (b):

  - In large areas, supply forms to enable placement of the LMC overlay and support them by blocking from the stringers.  If utilized in the original construction of the structure, existing stay in place forms that are in good condition will be sufficient to meet this requirement.

  - In small areas, supply forms to enable placement of the LMC overlay.  Forms may be suspended from existing reinforcing bars by wire ties.  If utilized in the original construction of the structure, existing stay in place forms that are in good condition will be sufficient to meet this requirement.

426.03.09 Limitation of Operations.

DELETE:	  The second paragraph in its entirety, “No traffic will be permitted … has reached 3000 psi.”

INSERT:  The following.

Do not apply loads to the bridge deck overlay until the final section of the overlay placed in the structure’s staged construction has completed its specified air curing period as specified in 426.03.07.  No vehicles, including heavy construction equipment, will be permitted on bridge deck overlay until the concrete cylinder breaks have attained a compressive strength of 3000 psi.  However, loads such as stored materials, lightweight equipment, and concrete safety parapets, may be placed upon the concrete slab via lifting devices after the air curing period.  Do not open the bridge deck overlay to traffic until concrete cylinder breaks have attained a compressive strength of 3000 psi, the air curing period is complete, the cracks are filled with an approved gravity fill polymer as specified in 426.03.07, and the overlay is grooved as specified in 426.03.08.