Category 400

Structures

SECTION 436 — Cleaning and Painting Existing Structural Steel

436.03 CONSTRUCTION

436.03.01 Submittals.

DELETE:  The first paragraph “Submit the following drawings, plans, and information…by the Administration” in its entirety.

INSERT:  The following.

Submit the following drawings, plans, and information for accomplishing the work.  Except for (e) below, submit electronic versions in Portable Document Format (PDF) on company letterhead to the Office of Structures, Structure Inspection, and Remedial Engineering Division via email at: oospaintcontracts@mdot.maryland.gov.  Do not proceed with the work until the submittals are approved by the Administration.

436.03.04 Inspection Equipment.

DELETE:  The first paragraph “Provide for the exclusive…of the Contract.” in its entirety.

INSERT:  The following.

Provide for the exclusive use of the Engineer, the following equipment and reference manuals for the QA observations of the cleaning and painting operations. Maintain, calibrate, and verify the equipment is in a condition that is satisfactory to the Engineer.  The equipment will remain the property of the Contractor at the conclusion of the Contract.

DELETE:  Paragraphs (d) and (j) in its entirety.

INSERT:  The following.

- Electric or Sling Psychrometer, 32 F to 106 F

- Digital Magnetic Dry Film Coating Thickness Gauge (SSPC-PA 2, Type 2) capable of transferring data to a laptop, tablet, or similar device through a wireless connection (i.e., “Bluetooth”), and storing at least 1000 readings.

436.03.10 Methods of Cleaning.

DELETE:  The “Methods of Cleaning” table.

INSERT:	The following:

| PAINT SYSTEM | SUBSTRATE | METHOD OF CLEANING |
| --- | --- | --- |
| C, D, I & J | Abrasive blast cleaned steel | Existing Paint to be Removed - Localized (a) and (b) and complete (h) |
| E & H | Overcoating existing paint | Existing Paint to be Overcoated - Localized (a) and complete (c) followed by (d) and (e) |

(h) Near White Metal Abrasive Blast Cleaning.

DELETE:  The second paragraph “Whenever the existing condition…specified above the profile”.

INSERT:  The following.

Whenever the surface profile exceeds 4.0 mils, apply the primer in no less than two coats to achieve the minimum dry film thickness specified above the peaks of the profile.

436.03.12 Removal of Vegetation, Planking, and Signage.

DELETE:  436.03.12 in its entirety.

INSERT:  The following.

436.03.12 Removal of Vegetation, Planking, Signage, and Cleaning of Drainage Troughs.  Prior to surface preparation, remove vegetation overhanging or fouling the structure and remove any accumulations of debris from inside the drainage troughs.

When the structure has planking (timber or plywood) between the beams, carefully remove it in the areas of work operations.  Existing planking that is in good condition may be used in the proposed planking operations. Store and maintain in good condition the existing planking that is to be reused.  Dispose of all debris on the planking and any planking that is not to be reused.  Unless otherwise directed, install the proposed planking after the cleaning and painting operations are complete.  The Engineer may direct that the existing planking be reinstalled, or the proposed planking be installed before opening lanes to traffic during that same working day.  The Engineer may also request that planking be installed or reinstalled during periods of work stoppage.  Reinstall the existing planking or install new planking in the same locations as the existing by following the details in the Contract Documents.  Cut any existing planking to fit the details as necessary.  Add any missing elements (additional plywood, timber beams, etc.) or replace poor elements with new timber as specified in 921.05.  																																																																																																																																																																											When the fascia webs of the structure contain street identification signs, remove them prior to starting cleaning operations in the area.  Clean and paint areas exposed by the sign removal, including bolt holes.  Whenever a sign is removed, notify the Engineer.  The Engineer will notify the Office of Traffic and Safety’s Chief, Traffic Operations Division.  Street signs may be reinstalled by the Office of Traffic and Safety utilizing the Contractor’s maintenance of traffic.  They will coordinate this work with the Contractor.

If drainage troughs are present, conduct a survey of the troughs prior to construction and document the condition of all trough materials.  Notify the Engineer of the locations where trough materials are in poor condition.  Clean all drainage troughs on the structure unless otherwise directed by the Engineer.  Replace drainage troughs as directed by the Engineer.  Support the weight of the trough material to prevent tearing during removal.  Remove any hardware used to attach the trough to the structure (e.g.- nuts, bolts, brackets, and fittings) Store and maintain the hardware so that it may be reused when reinstalling the troughs.  Remove and properly dispose of any accumulations of debris from inside the trough.  Upon completion of cleaning, re-attach the trough material in the same manner it was removed.  Overlapping pieces of trough material must maintain the same pattern of overlap as when they were removed.  Regardless of whether troughs are removed, replaced, or cleaned, ensure that no paint related debris is present within the troughs at the completion of painting operations.

436.03.19 Weather Requirements for Painting.

DELETE:  Paragraph (c) in its entirety, “The ambient…40 F.”

INSERT:  The following.

(c) 	The ambient temperature in the shade is above 40 F or the minimum temperature specified by the manufacturer, whichever is greater, and will be constant or higher until the paint cures to readiness for recoating by meeting the manufacturer’s requirements.

DELETE:  Paragraph(e) in its entirety, “The surface temperature…top coated.”

INSERT:  The following.

(e) The surface temperature is a minimum of 5 F above the dew point and will be constant or higher until the paint cures to readiness for recoating as specified by the manufacturer.

436.03.21 Application of Prime, Intermediate, and Finish Coats.

DELETE:  The “Stripe Coat Application Schedule” table.

INSERT:  The following.

| SYSTEM | COAT |
| --- | --- |
| B | II & III |
| C | I* & II |
| E | I & II |
| H | II & III |
| I | I* & II |

436.03.28 Field Cleaning Containment System Plan Guidelines.

DELETE:  Paragraph (h) in its entirety.

INSERT:  The following.

(h) Prepare and submit all drawings requiring a professional engineer review and seal as defined in (g) above as specified in Section 499.  Submit electronic versions of drawings in Portable Document Format (PDF).  Provide the submittal on company letterhead.  Drawings not requiring a professional engineer review and seal may be formatted for printing on standard paper size (8- 1/2in. x 11 in.).  Drawings that do require a professional engineer review and seal shall be submitted by the engineer responsible for its design and be formatted for printing on paper which is 11 in. x 17 in. or greater.  When a professional engineer stamp is required, sign and seal each sheet by the professional engineer.

ADD:  The following after paragraph (j).

(k) When the structure is over another road, and the road below the work area is open to traffic, provide details in the drawings to show the specific measures which will be taken during the installation and removal of the containment system to prevent tools, equipment, and materials from falling to the roadway below.  Demonstrate the effectiveness of the proposed measures before performing the work. Immediately stop work if the proposed measures become ineffective.

436.03.31 Worker Protection Compliance Program.

DELETE:  The first paragraph “436.03.31 Worker Protection Compliance Program.  The Worker Protection Compliance Program shall be…” in its entirety.

INSERT:  The following.

436.03.31 Worker Protection Compliance Program.  The Worker Protection Compliance Program shall be on company letterhead and meet OSHA and the MOSH - Lead in Construction Standards, and other applicable toxic metal standards.  The Worker Protection Compliance Program shall be reviewed, signed, sealed and submitted by the CIH or CSP who conducted the review.  The Worker Protection Compliance Program shall include a commitment for the CIH or CSP, or a person working under the direction of CIH/CSP, to provide written certification each month of compliance with the Worker Protection Compliance Program, including biological monitoring.  Provide a copy of the letter within 6 working days after the end of the month.

436.03.33 Environmental Protection Plan of Action (EPPA).

DELETE:  The first paragraph “436.03.33 Environmental Protection Plan of Action (EPPA).  An EPPA confirming that the environment…monitoring air, soil, and water” in its entirety.

INSERT:  The following.

436.03.33 Environmental Protection Plan of Action (EPPA).  An EPPA confirming that the environment is protected from contamination is required when the coatings are being abrasive blast cleaned (regardless of the presence of toxic metals), or the coating being disturbed contains toxic metals (regardless of the method of preparation).  When an EPPA is required, it shall be reviewed, signed, sealed, and submitted by the CIH or CSP who conducted the review and shall include procedures for monitoring air, soil, and water.

436.03.34 Methods for Assessing Emissions.

DELETE:  Paragraph (b)(1) “Abrasive Blast Cleaning” in its entirety.

INSERT:  The following.

- Abrasive Blast Cleaning.  Begin daily ambient air monitoring at least one day prior to beginning work at each structure where abrasive blast cleaning is to occur.  Continue daily ambient air monitoring during the first 10 days of productive abrasive blast cleaning operations.  When the results indicate that the containment is controlling emissions, full-time monitoring may be discontinued unless otherwise directed.  At the conclusion of every 30 calendar day period from the last day of monitoring, repeat monitoring for 2 consecutive days of productive abrasive blast cleaning.  Except for on the first day of monitoring, conduct ambient air monitoring only during the work shift while blast cleaning or other dust producing operations are underway.

Monitor the ambient air full-time if the results of the monitoring during the initial 10 days, or from the periodic 30 calendar days are found to be unacceptable.  When the results indicate the containment is controlling emissions and when approved, periodic 30 calendar days monitoring may be initiated or resumed.  Resume full-time monitoring when unacceptable visible emissions or residues are observed on the ground or water and as directed.

436.03.36 Waste Handling Plan of Action.

DELETE:  The first paragraph “436.03.36 Waste Handling Plan of Action.  Required for the handling, storage, and disposal…an original seal” in its entirety.

INSERT:  The following.

436.03.36 Waste Handling Plan of Action.  Required for the handling, storage, and disposal of all hazardous waste, regardless of the presence of toxic metals.  When the project involves the removal of paint containing toxic metals, the program shall be reviewed, signed, sealed and submitted by the CIH or CSP who conducted the review.

ADD:  The following after 436.03.41 Nonhazardous Waste Disposal.

436.03.42 Health and Safety Plan.  Submit a site specific Health and Safety Plan on all projects where coatings removal or application occurs.  The Health and Safety Plan shall address all anticipated project specific hazards, the policies implemented to address the hazards, identify the contractor’s on-site competent person, and provide emergency procedures to be followed, including emergency contact requirements and directions to the nearest emergency care facility. Provide concepts and calculations for fall protection systems which are manufactured or assembled on site.

436.04 Measurement and Payment

DELETE:  436.04 in its entirety.

INSERT:  The following.

436.04 Measurement and Payment

The Contract unit price for the item specified will be full compensation for all cleaning and painting, scaffolding, platforms, containment systems, permits, working drawings, daily quality control records, professional engineer’s services used for containment, industrial hygienist services, air monitoring, sampling and testing of materials for toxic metal content, including any revisions and resubmissions that may be required during the execution of the work, providing safe access for inspections, hand wash station/decontamination area, floodlighting, test plates, drums, collection and storage at the temporary storage site, hauling and disposal at an approved industrial waste site or hazardous waste site, removal of debris, and all material, labor, equipment (including test equipment), tools, and incidentals necessary to complete the work.

    - Cleaning and painting existing structural steel will not be measured but will be paid for at the Contract lump sum price for the pertinent cleaning and painting items.

    - All costs associated with the repair of existing coatings due to new construction, structural repairs, and damage caused by the Contractor’s operations will not be measured but will be incidental to the pertinent repair items, structural steel items, or cleaning and painting items.

    - Cleaning of Drainage Troughs will not be measured but will be incidental to the pertinent cleaning and painting items.  The payment will be full compensation for all material, labor, equipment, tools, and incidentals necessary to complete the work.

    - Repair and Replacement of Existing Drainage Troughs will be measured and paid for at the Contract unit price per linear feet.  The payment will be full compensation for all material, labor, equipment, tools, and incidentals necessary to complete the work.

    - Timber Planking will be measured and paid for at the Contract unit price per square foot.  The payment will be full compensation for the removal of existing planking, removal, and disposal of debris on existing planking, storage of existing planking materials to be reused, modification to existing planking, new planking, construction and installation of proposed planking and all material, labor, equipment, tools, and incidentals necessary to complete the work.