Category 400

Structures

SECTION 440 — Prestressed Concrete Beams and Slab Panels

440.02 MATERIALS

ADD:  The following at the end of materials list.

| Epoxy Protective Coatings | 917.01 |
| --- | --- |
| Epoxy Grout | 902.11(d) |

440.03 CONSTRUCTION

440.03.13 Steel Strand Tensioning.

DELETE: The fifth paragraph “Cut all pretensioned steel…. All voids into the strands.”

ADD:  The following:

440.03.15 Detensioning.

(c) Cutting and Protecting Strand Ends.  After the beams or slab panels have been detensioned, clean the ends of the strands to remove all foreign material such as rust, slag, grease, etc until the surface is visibly clean and water break free.  Use wire brushing or abrasive blast cleaning to remove all dirt and residue that is not firmly bonded to the metal and concrete surfaces.  Work a protective coating into all voids of the strands using the following methods:

- Where strands in beam or slab ends are to ultimately be encased in a concrete deck or end section, cut the strands flush with the concrete end.  Prepare the surface and apply an epoxy protective coating to the strands and adjacent concrete as specified in Section 464.  Extend the limits of the coating a minimum of 1 inch beyond the strand perimeter at each strand location.

- Where strands in beam or slab ends are to be exposed to the air, recess the cuts a minimum of 1/2 inch into the end of the beam.  Fill the recessed area with an approved epoxy grout conforming to 902.11(d) in accordance with the manufacture’s recommendations.  Match the surface finish of the epoxy gout to that of the beam end.  Prepare the surface and coat the entire end of the beam with an epoxy protective coating as specified in Section 464.

- If the end of the beam or slab will bear on a substructure unit directly under a bridge deck joint, protect the ends as specified in 440.03.15(c)(2).  Prepare the surfaces and coat the bottom of the top flanges, the web, and bottom flanges for an additional five feet beyond the end of the concrete member with the same epoxy protective coating as specified in Section 464.