CATEGORY 500

PAVING

SECTION 510 — Sealing Cracks and Joints in Asphalt Pavements

510.03 CONSTRUCTION

510.03.07.02 Crack Sealing with Routing.

DELETE:  510.03.07.02(a).

INSERT:  The following.

- Crack Routing.  Perform routing of cracks to form a reservoir with a cut centered in the crack, touching each side of the crack, with a resulting width ranging from 0.5 in. to 1 in., depending on the width of the crack.  The depth shall be 3/4 in. Perform routing in such a way that the pavement does not spall, thus allowing for optimal adhesion of the sealant to the crack edges.  The reservoir should be square or U-shaped, not worn to a V-shape.

510.03.08.01 Crack Sealing.

DELETE:  510.03.08.01(c).

INSERT:  The following.

- Installation.  Two methods can be used for crack sealing.  The crack shall be sealed using the flush fill method with a squeegee finish or by placing an overband.  The width of the overband should not extend more than 2 in. and should be no more than 1/20 in. thick, or the thickness of a dime.  Keep sealant narrow and tight to the pavement to minimize snowplow damage.  Perform material handling and installation in accordance with the manufacturer’s instructions.

510.04 MEASUREMENT AND PAYMENT

DELETE:  510.04.01 and 510.04.02 in its entirety.

INSERT:  The following.

510.04.01 Crack Sealer without Routing will be measured and paid for at the Contract unit price per linear foot, per lane mile, or per pound as specified.

510.04.02 Crack Sealer with Routing will be measured and paid for at the Contract unit price per linear foot, per lane mile, or per pound as specified.

510.04.03 Asphalt Repair Mastic will be measured and paid for at the Contract unit price per gallon.