Category 900

Materials

SECTION 909 — Metals

ADD: The following after 909.11.

909.12 METAL REINFORCED EPOXY FILLER.

METAL REINFORCED EPOXY FILLER.  The metal reinforced epoxy filler shall be a metal reinforced epoxy/polymeric compound that is designed to rebuild, restore, and repair metal surfaces.  The manufacturer shall furnish actual test results for each batch of epoxy filler submitted showing the following:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Compressive Strength (psi) | D 695 | 8000 |
| Adhesive Tensile Shear Strength (psi) | D 1002 | 900 |
| Flexural Strength (psi) | D 790 | 5000 |
| Specific Gravity | D 792 | 1.5 – 2.5 |
| Cured Hardness, Durometer (Shore D) | D 2240 | 80 ± 5 |
| Cured Shrinkage (%) | D 2566 | < 1 |
| Color | — | Grey or Black |