Category 900

Materials

SECTION 911 — Joints

911.01 JOINT SEALER AND CRACK SEALER

DELETE:  911.01.02 Asphalt Repair Mastic in its entirety.

INSERT:  The following.

911.01.02 Asphalt Repair Mastic.  Asphalt repair mastic shall be composed of quality-selected asphalt and/or resins, select aggregates with structural integrity, synthetic rubber polymers, antioxidants, naturally occurring and man-made reinforcing material, and other modifiers.  The aggregate and polymer modified binder shall be pre-measured and packaged in a plastic bag but shall not be pre-mixed and the weight of mastic should be within 12 lb/gal to 16 lb/gal range. Asphalt repair mastic shall meet ASTM D8260 Type II and the following.

| MATERIAL | PHYSICAL PROPERTIES | TEST | LIMITS |
| --- | --- | --- | --- |
| Asphalt Repair Mastic | Shelf Life | — | 2 years |
|  | Pot Life | — | 12 hours maximum |
|  | VOC, g/l | — | 0 |
| Asphalt Binder | Cone Penetration, 77 F (25 C) | D5329 | 70 Maximum |
|  | Cone Penetration, 122 F (50 C) | D5329 | 120 Maximum |
|  | Softening Point (R&B) | D36 | 200 F (93.33 C) Minimum |
| Aggregate | Aggregate, Factory Blended in Compound | D5444 | 100% Passing 5/8 in. 8% Passing #200 Maximum |
| Mix Design | Tensile Adhesion, psi (kPa) | D5329 Modified1 | 15 psi (83 kPa) Minimum, 0.5 in. (12 mm) Minimum Elongation |
|  | Impact Testing, 5/8 in. dart, 2 in. (50 mm) Diameter 1 in. (25 mm) Thick Specimen | D2794 | No Cracking, Chipping or Separation at 6 ft-lb, at 20 F |
|  | Flexibility | D5329 Modified2 | No Cracking or Loss of Aggregate Adhesion |

Notes:

1. The specimen for the tensile adhesion is 3 in. long x 2 in. wide x 1.5 in. thick.

2. The specimen is 6 in. x 4 in. at 20 mm thickness.  The test is run at 77 F and bent over a 1 in. mandrel to 180 F over 10 seconds.

ADD:  The following after 911.01.02.

911.01.03 Pourable Silicone Joint Sealant for Structures.  Pourable silicone sealant for roadway joints in structures shall be a two component, cold applied, rapid cure (accommodate thermal and vertical traffic movements within 8 hours), self-leveling, 100 percent mixed together.  A VOC compliant primer will be used throughout all applicable tests when recommended by the manufacturer.

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Part A |  |  |
| Specific Gravity | D 792 | 1.2-1.4 |
| Extrusion Rate (ml/minute) | C 1183, Type S | 50 minimum |
| VOC (g/L) | — | 50 |
| Color | — | Dark Grey |
| Part B |  |  |
| Specific Gravity | D 792 | 1.3-1.6 |
| VOC (g/L) | D 3960 | 0 |

The material shall conform to the following requirements when mixed and applied at 77 F and 50 percent relative humidity:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| As Cured (Joint size = 1/2 inch x 1/2 inch x 2 inches) |  |  |
| Skin-Over Time (minutes) | — | 20 |
| Tack-Free Time (minutes) | C 679 | 30-60 |
| Cure (hours) | — | 8 |
| Hardness, Durometer (Shore A2) | C 661 | 25 maximum |
| Joint Elongation (%) | D 412, Die C | 600 minimum |
| Joint Modulus @ 150% elongation (psi) | D 412, Die C | 8-12 |
| Joint Movement (%) | C 719 | +100/-50 |
| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| Operating Temperature Range (F) | — | -50 to 300 |
| Accelerated Weathering (hours) | C 793 | 5,000 |

Each container of silicone joint sealant shall have a minimum shelf life of six months, and material more than six months old shall be retested prior to use.

911.01.04 Preformed Silicone Joint Seal. The manufacturer shall furnish certification showing that the preformed silicone joint seal meets the following:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Specific Gravity | D 792 | 1.3-1.6 |
| Hardness, Durometer (Shore A) | D 2240 | 55 ± 5 |
| Tensile Strength (psi) | D 412, Die B | 750 |
| Elongation (%) | D 412, Die B | 350 |
| Tearing Strength (lbs./in.) | D 624, Die B | 80 |
| Compression Set (%) @ 350º F, 72 hrs. | D 395 | 30 |
| Heat Aged Properties (change %) (Hardness, tensile strength, elongation) | D 573 | 10 maximum |
| Operating Temperature Range (F) | — | -50 to 300 |
| Color | — | Black |

911.01.05 Silicone Adhesive.  The manufacturer shall furnish certification showing that the non-sag, high modulus silicone adhesive meets the following at 77 F and 50 percent relative humidity:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Sag/Flow (in.) | C 639 | 0.20 maximum |
| Skin Over Time (minutes) | — | 5-10 |
| Tack Free Time (minutes) | C 679 | 30 maximum |
| Cure, 1/4 in. thickness, (hours) | C 679 | 24 maximum |
| Hardness, Durometer (Shore A2) | C 661 | 25 maximum |
| Elongation (%) | D 412 | 450 minimum |
| Tensile Strength (psi) | D 412 | 200 minimum |
| Resistance to UV | C 793 | No Cracking, Chalking or Degradation |
| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| Peel Adhesion to Substrates (lbs./in.) | C 794 | 50 minimum |
| VOC | D 3960 | 0 |

911.01.06 Non-Sag Silicone Sealant for Vertical Joints in Structures.  Non-sag silicone sealant for vertical joints in structures shall be a one-part, cold applied, non-sag silicone sealant material that cures to a weather and UV resistant low-modulus silicone rubber upon exposure to atmospheric moisture.

The material shall conform to the following requirements when applied and cured for 21 days at 77 F and 50 percent relative humidity:

| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| --- | --- | --- |
| Specific Gravity | D 792 | 1.3-1.6 |
| Slump (in.) | D2202 | 0.30 maximum |
| Extrusion Rate (ml/minute) | C 1183 | 20 maximum |
| Skin-Over Time (minutes) | — | 60 maximum |
| Tack-Free Time (hours) | C 679 | 5 maximum |
| Hardness, Durometer (Shore A2) | C 661 | 25 maximum |
| Tensile Stress @ 150% elongation (psi) | D 412, Die C | 45 maximum |
| Elongation (%) | D 412, Die C | 600 minimum |
| Joint Movement (%) | C 719 | +100/-50 |
| Heat Aged Properties (change %) (hardness, tensile strength, elongation) | C 792 | 10 maximum |
| Accelerated Weathering (hours) | C 793 | 5,000 |
| Color |  | Grey or Black |

No cracks or separation is allowed after the material is cured.

Each container of silicone sealer shall have a minimum shelf life of six months. Material more than six months old shall be retested.

ADD:  The following after 911.12.

911.13 PREFORMED FOAM SEALS

911.13.01 Closed Cell Foam Joint Seal.  Use a low density, closed cell, cross-linked, ethylene vinyl acetate polyethylene copolymer preformed foam that is physically blown using nitrogen, and is impermeable, weather and wear resistant, waterproof and chemical resistant, hold in temperature extremes of -94 F to 158 F, and meeting the following:

| PROPERTY | REQUIREMENT | TEST METHOD |
| --- | --- | --- |
| Density | 2.5 – 3.5 lb/ft3 | D 545 |
| Tensile, min | 70 psi | D 3574 |
| Water Absorption, max by volume | (0.02) 0.07 | MIL SPEC. P-40619 |
| Tear Strength, min | 13 psi | D 624 |
| Chemical Resistance | — | D 543 |

Place grooves on the foam seal along the bond surfaces at a distance of 1/4 in. to 1/2 in. apart.  Ensure the grooves have an approximate dimension of 1/8 in. wide by 1/8 in. deep and run the entire length of the joint.

911.13.02 Adhesive.  Use a two component, 100 percent solid, modified epoxy adhesive designed for bonding the joint seal to steel.  Obtain the adhesive from the seal manufacturer that is fully compatible with the foam joint seal material in accordance with the manufacturer’s specifications.