Category 400

Structures

SECTION 423 — Repairs to Concrete Structures

423.02 MATERIALS

423.02.02 Concrete for Structural Repairs (Not Including Bridge Decks).

INSERT: The following at the end.

If the quantity of concrete to be used in a single day is low (less than 2 cubic yards) or in areas where concrete delivery is impractical, the contractor has the option to mix the concrete on site in lieu of receiving it from a ready-mix plant.  Mix No. 5 concrete can be replaced with a mixture of non-shrink grout and pea gravel proportioned and mixed in accordance with the manufacturer’s recommendations. This substitution is subject to the approval of the engineer and is at no additional cost to the Administration.