CATEGORY 400

STRUCTURES

SECTION 436 — Cleaning and Painting Existing Structural Steel

436.03 CONSTRUCTION

436.03.21 Application of Prime, Intermediate, and Finish Coats.

DELETE:  The fourth paragraph of 436.03.21 in its entirety, “Maintain, calibrate, and adjust… according to the following schedule”.

INSERT:  The following.

Maintain, calibrate, and adjust the thickness measuring instrument, and take measurements according to SSPC-PA 2.  Apply stripe coats using brush, dauber, or roller to all edges, outside corners, crevices, welds, rivets, bolts, nuts, washers, and rough and pitted surfaces prior to the application of coatings according to the following schedule:

436.03.26 Final Identification.

DELETE:  436.03.26 Final Identification in its entirety

INSERT:  The following.

436.03.26 Final Identification.  Once the final coat of paint has cured, apply as many as two “paint system” stencils for each paint system which was applied.  On the paint system stencil, identify the paint system letter designation used, the product manufacturer of the paint system, the specification numbers in Section 912 for each coat of paint, and the month and year in which the application was completed.  Use black numbers and letters which are 2 in. to 2-1/2 in. high that are made of a material which is compatible with the paint system and which will not run, fade, or otherwise become illegible due to atmospheric exposure.  Apply the paint system stencils to the inside surfaces of fascia beams near the abutments at specific locations selected by the Engineer.  When more than one paint system is used, apply additional paint system stencils.

If the existing coating system was not fully removed from the entire bridge, ensure that the existing coating information (when available) is visible on the bridge after all work is complete.  This may require installing new stencils for the existing system in areas designed by the Engineer.

When bridge identification details are included in the contract documents, apply the bridge identification number to the bridge in accordance with Section 495 at the specific locations selected by the Engineer.

436.03.34 Methods for Assessing Emissions.

DELETE:  The first paragraph of 436.03.34(a) in its entirety, “SSPC Level 1 Visible Emissions.  The following Level 1 visible emissions… or power tool cleaning”.

INSERT:  The following:

- SSPC Level 1 Visible Emissions.  The following Level 1 visible emissions criteria apply when any dry method of surface preparation is performed, such as dry abrasive blasting or power tool cleaning.

DELETE:  436.03.34(b) in its entirety, “Ambient Air Monitoring.  Unless otherwise directed… or 7 hours, whichever is greater”.

INSERT:  The following.

- Ambient Air Monitoring.  Unless otherwise directed, ambient air monitoring is required when any dry method of surface preparation is performed, such as dry abrasive blasting or power tool cleaning.  Ensure monitoring starts one half hour before blast cleaning or power tool cleaning begins and continues for the entire duration of the cleaning activity or seven (7) hours, whichever is greater.

436.04 MEASUREMENT AND PAYMENT

DELETE:  The first paragraph of 436.04 in its entirety, “The Contract unit price… to complete the work”.

INSERT:  The following.

The Contract unit price for the item specified will be full compensation for all cleaning and painting, scaffolding, platforms, containment systems, permits, working drawings, daily quality control records, professional engineer’s services used for containment, industrial hygienist services, air monitoring, sampling and testing of materials for toxic metal content, including any revisions and resubmissions that may be required during the execution of the work, providing safe access for inspections, hand wash station/clean up area, floodlighting, test plates, drums, collection and storage at the temporary storage site, hauling and disposal at an approved industrial waste site or hazardous waste site, removal of debris, installing paint system stencils and bridge identification number,  and all material, labor, equipment (including test equipment), tools, and incidentals necessary to complete the work.