Category 900

Materials

SECTION 900 — General

900.03 RECYCLED MATERIALS

ADD:  The following after 900.03.02, (c) Drainage Systems.

- Base course under permeable pavements.

- Longitudinal underdrains.

- Base course and Subbase within 3 ft of Longitudinal underdrains.

ADD:  The following at the end of the last sentence in subsection 900.03.03 RECYCLED ASPHALT PAVEMENT (RAP)

900.03.04 DREDGED MATERIAL (DM) and DREDGED MATERIAL BLENDS (DMB)

Definitions.

Dredged Material (DM).  Material excavated or dredged from the waters of the State as referenced in COMAR 26.04 and COMAR 26.10.13.  The term "waters of this State" is also specifically defined in COMAR.  It includes a wide range of surface and underground waters within Maryland's jurisdiction, such as surface and underground waters within state boundaries, the Chesapeake Bay and its tributaries, and various bodies of water and drainage systems like ponds, lakes, rivers, and streams.  It also encompasses the portion of the Atlantic Ocean within the state's boundaries and the floodplain of free-flowing waters as determined by the Department based on the 100 year flood frequency.  The DM includes Sand, Silt, Clay, Gravel, Mud, Muck, Rock or other sediment or material excavated or dredged from tidal, estuarine, or riverine waters of the State, including potentially dry areas at the time of excavation beneath the plane bounded by the normal high water line.  DM includes but is not limited to dredged slurry, hydraulic fill, or dewatered dredged material from fresh, brackish, or saltwater environments.

Dredged Material Blend (DMB):  A homogeneous mixture of dredged material with other approved borrow materials.

Corrosivity, Gradation and Toxicity Requirements.  DM and DMB shall meet the following requirements:

| Parameter | Acceptable Range | Test Method |
| --- | --- | --- |
| Minimum resistivity (Ω·cm) | > 3,000 | T 288 |
| pH | 5.5 – 8.5 | T 289 |
| Sulfate content (ppm) | < 500 | T 290 |
| Chloride content (ppm) | < 400 | T 291 |
| PFOA and PFOS Organic Content | < 4 ng/L (in leachate) < 8% | EPA Method 1633 with D 3987 (Leaching) T 267 |
| Gradation % Passing #200 Sieve | ≤ 30% | T 11 |

Notes: Ω·cm = ohm·centimeter,

ppm = parts per million.

PFAS = Perfluoroalkyl and Polyfluoroalkyl substances

PFOA = Perfluorooctanoic Acid

PFOS = Perfluorooctane Sulfonate

In addition to the above requirements, DM and DMB shall follow the procedures and meet the requirements of Category 1 – Residential Unrestricted Use Soil and Fill Material or Category 2 – Non-Residential Restricted Use Soil and Fill Material land use categories as specified by Maryland Department of the Environment (MDE) in the current Innovative Reuse and Beneficial Use of Dredged Materials (IRBDM).  All MDE requirements shall be satisfactorally met, including but not limited to the screening process, sampling, frequency of sampling, and testing analysis with a listing of the appropriate test procedures.  It is the contractor’s responsibility to obtain the MDE approval, whether directly or indirectly from the source vendor, satisfactorily demonstrating that all MDE requirements are met.

DMB requires blending DM, as necessary, with soil, quarry fines or other materials to meet the above requirements.  The DMB will be subject to a blending study done by the contractor or supplier.  The blending study will be outlined in the Sampling and Analysis Plan (SAP) which will be reviewed and approved by MDE within 30 days.  Test the blending material(s) in accordance with all MDE IRBDM testing requirements.  SHA will only sample and test the final blend for the final approval of the material after receiving approval and test results per the IRBDM.  Source submissions will be considered with an approved Sampling and Analysis Plan (SAP) from MDE if a blending study was conducted.  Provide a declaration of potential environmental impacts to adjacent properties and a Confirmation of Suitability of use / Interim Receiving Site Form containing the following information:

- MDE Tracking Number.

- Land Use Category.

- Volume of Material.

- The End User/Interim Receiving site a “Groundwater Use Area” has been determined.

- Both forms must have the appropriate signatures.

Usage.  Use DM and DMB as Common, Select or Modified Borrow provided DM and DMB meet the requirements of 916.01, 204.02, MDE IRBDM, and the Corrosivity, Gradation and Toxicity Requirements above.  An additional written consent by the Administration is required prior to DM or DMB use.  Do not use DM and DMB for the following:

- Portland cement concrete.

- Hot mix asphalt.

- Mechanically stabilized earth (MSE) systems:

  - MSE walls.

  - Reinforced soil slopes (RSS).

  - Reinforced earth slopes (RES).

- Within 500 feet of any potable water supply wells.

- Within karst geologic terrain.