Category 900

Materials

SECTION 902 — Portland Cement Concrete and Related Products

902.10.03 Portland Cement Concrete Mixtures.

DELETE: The 	TABLE 902 A in its entirety.

INSERT: The following.

TABLE 902 A

| PORTLAND CEMENT CONCRETE MIXTURES |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MI X NO. | SPECIFIED ACCEPTANCE COMPRESSIVE STRENGTH psi | COMPREHENSIVE STRENGTH ACCEPTANCE TEST AGE days | STD. DEV. psi | CRITICAL VALUE psi | MIN CEMENT FACTOR lb/yd3 | COARSE AGGREGATE SIZE M43 / M195 | MAX WATER/CEMENT RATIO by wt | SLUMP RANGE in. | TOTAL AIR CONTENT % | CONCRETE TEMP. °F. |
| 1 | 2500 | 28 | 375 | 2430 | 455 | 57, 67 | 0.55 | 2 - 5 | 5 - 8 | 50 - 95 |
| 2 | 3000 | 28 | 450 | 3010 | 530 | 57, 67 | 0.50 | 2 - 5 | 5 - 8 | 50 - 95 |
| 3 | 3500 | 28 | 525 | 3600 | 580 | 57, 67 | 0.50 | 2 - 5 | 5 - 8 | 50 - 95 |
| 4 | 3500 | 28 | 525 | 3600 | 615 | 57, 67 | 0.55 | 4 - 8 | N/A | 50 - 95 |
| 5 | 3500 | 28 | 525 | 3600 | 580 | 7 | 0.50 | 2 - 5 | 5 - 8 | 50 - 95 |
| 6 | 4500 | 28 | 675 | 4770 | 615 | 57, 67 | 0.45 | 2 - 5 | 5 - 8 | 50 - 80 |
| 7 | 4200 | 28 | 630 | 4420 | 580 | 57 | 0.50 | 1½ - 3 | 5 - 8 | 50 - 95 |
| 8 | 4000 | 28 | 600 | 4180 | 750 | 7 | 0.42 | 2 - 5 | 5 - 8 | 50 - 80 |
| 9 | 3000 | (a) | N/A | N/A | 800 | 57, 67 | 0.45 | 4 - 8 | 5 - 8 | 60 - 100 |
| 10 | 4500 | 28 | 675 | 4770 | 700 | ¾" - No. 4 | 0.45 | 2 - 5 | 6 - 9 | 50 - 80 |
| 11 | 4200 | 28 | 630 | 4420 | — | 57, 67 | 0.45 | 2 - 5 | 5 - 8 | 50 - 80 |
| 12 | 4200 | 28 | 630 | 4420 | — | ¾" - No. 4 | 0.45 | 2 - 5 | 6 - 9 | 50 - 80 |
| 13 | 4000 | 28 | 600 | 4180 | 615 | 57, 67 | 0.45 | 2 - 5 | 5 - 8 | 50 - 95 |
| HE | 3000 | (b) | N/A | N/A | N/A | N/A | N/A | 3 - 9 | 5 - 8 | 60 - 100 |
| PC (c) | N/A | N/A | N/A | N/A | 450 | 7, 8 | 0.45 | N/A | 15 - 25 | N/A |
| WT | 2500 | (d) | N/A | N/A | 650 | 57 | 0.45 | 5 max | 5 - 8 | 50 - 95 |