Category 900

Materials

SECTION 916 — Soil and Soil Aggregate Borrow

916.01 BORROW EXCAVATION

DELETE:  The BORROW REQUIREMENTS table.

INSERT:  The following as the BORROW REQUIREMENTS table, with additional note No. 5.

| BORROW REQUIREMENTS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Class Borrow | Max Dry Density Minimum P.C.F. T 180 | LL Maximum T 89 | PI Maximum T 90 | Gradation Requirements T 88 | Reference MSMT Soil Classification | Reference AASHTO Classification |
| Select Borrow | 105 | 34 | 7 | 30% max passing No. 200 sieve | A-2, A-3, A-2-4 | A-1-a, A-1-b, A-3, A-2-4 |
| Capping Borrow | 105 | 34 | 7 | 30% max passing No. 200 sieve 1 | A-2, A-3, A-2-4 | A-1-a, A-1-b, A-3, A-2-4 |
| Modified Borrow | 125 | 30 | 9 | 50% min retained on No. 4 sieve | Any material except A-5 | A-2-4, A-4 2 |
| Common Borrow | 100 | N/A | N/A | N/A 5 | N/A | N/A |
| Clay Core3 | 100 4 | N/A | N/A | 30% min passing No. 200 sieve | N/A | N/A |
| 1 When material has no liquid and plastic limit and the amount of material passing the No. 4 sieve and retained on the No. 10 sieve is less than 10 percent of the total sample mass, the material shall have at least 15 percent passing the No. 200 sieve. 2 A-4 material must be a manufactured product. 3 Unified Soil Classification GC, SC, CH, or CL free of roots, stumps, wood, rubbish or other objectionable materials. 4 Test according to T-99-C 5 When Dredged Material or Dredged Material Blend is used as common borrow, the gradation requirements shall be 30% maximum passing No. 200 sieve and it meets the contamination level requirements. |  |  |  |  |  |  |