Office of Materials Technology

Landscaping Soils Procedure

Soils and Aggregate Technology Division

7450 Traffic Drive

Hanover, Maryland 21076

Landscaping Soils Eligibility Procedure and Producers List

Contacts

Dr. Intikhab Haider, Division Chief

443-572-5162 or ihaider2@mdot.maryland.gov

Amanuel Welderufael, Assistant Division Chief Lab Operations 443-572-5276 or awelderufael@mdot.maryland.gov

Benjamin Knipe, EIT., Soils Lab Team Leader

443-572-5055 or bknipe@mdot.maryland.gov

Toll Free:  866-926-8501

# Maryland Department of Transportation State Highway Administration

# Landscaping Soils Eligibility Procedure

# INTRODUCTION

Maryland Department of Transportation, State Highway Administration (the Administration) has the responsibility to effectively and efficiently assure the quality of landscaping soils used on the Maryland roadway system. Products placed must meet the system preservation, safety and environmental needs of the state's communities.  The Administration publishes this Landscaping Soils Eligibility procedure  as a tool for providing information and guidance on how, to become an MDOT SHA eligible producer of landscaping soils, and the quality of landscaping soils used on Maryland road projects can be assured.

This document  contains a list of landscaping soil producers (producers) whose Furnished Topsoil and/or Bioretention Soil Mix (BSM) are qualified for use on the Administration’ projects. The prequalified list will be updated and published on a quarterly basis. The eligibility of producers will be valid for one year; however, the nutrient management plan (NMP) will be valid for six months with an expiration date of  September 30th and March 31st respectively. The products that are qualified will be listed in the producers’ qualified list. Failure to meet the SHA specification after testing on three samples of same product (topsoil/BSM) will cause delisting of that product and/or producer from the list. The producer may be brought back in the eligibility list in next publication provided material (s) meets the MDOT SHA Specification.

The Administration encourages producers to keep track of their records, including due dates in order to submit their requests for renewal on time.  Producers are responsible for informing the Soils and Aggregate Technology Division (SATD) of any changes to producer information, such as producer name, location of stockpiles, subsidiary producer’s name, and contact information.

There will be an annual submittal period beginning forty-five days prior to the last day in July (i.e. June 15). You may become an eligible producer at any time in the year however your eligibility will expire on the last day in July regardless of when you submit your information.

# Process for prodUcer Listing as an Eligible Source of Landscaping Soils

  - PRODUCER REQUIREMENTS

    - Submission of Written Request

The producer shall submit a written request to be considered as an eligible source of landscaping soils to:

Dr. Intikhab Haider- Division Chief

Soils and Aggregate Technology Division

Maryland State Highway Administration

Office of Materials Technology

7450 Traffic Drive

Hanover, MD 21076 OR

ihaider2@mdot.maryland.gov

- The Administration requires producers to submit their written requests no later than 45 days prior to the next landscaping soils Eligibility List publication date. Failure to do so may cause delay in enlisting of producer in the next publication of eligibility list.  ”

- Please refer to Appendix A for “Landscaping Soils Producer’s Information Form. Producers shall complete and submit this form for each landscaping material produced (i.e. Bioretention Soil Mix and Furnished Topsoil).

2.1.2	Material Sampling and Testing

- A soil sample shall be taken per  ASTM D 75 to accurately represent the designated area within the site or stockpile. It is the producer’s responsibility to save a portion of this sample for QA testing by the Administration.

- The sample shall be labeled with the following information:

- Date of sampling.

- Name of the producer and contact phone number.

- Identify whether the sample is to be tested as furnished topsoil or BSM.

- The Producer shall submit the labeled landscaping soil sample to an accredited soil testing laboratory recognized by the Administration for testing.

- The list of recognized Soil Testing Laboratories can be found on the SHA Internet at the following address:

https://www.roads.maryland.gov/mdotsha/pages/index.aspx?PageId=52

- The testing laboratory may reduce the composite 10-pound sample, in accordance with AASHTO R-76 , to a minimum of one pound.

2.2	ADMINISTRATION RESPONSIBILITIES

- SATD will review the soil test results from the recognized lab of the producer’s choice (see link above for recognized labs) to determine if the material conforms to the Administration’s requirements (Table 1 and Table 2).

If the furnished topsoil/BSM test results are acceptable, SATD will send a response to the Producer indicating that the material is eligible to be tested for use on Administration projects.  The response will also indicate the expiration date of that eligibility.

3		TESTING PROCEDURES

The soil testing laboratory recognized by the Administration shall determine the following:

- Grading Analysis (R 58)

- Textural Analysis (T 88)

- Soil pH (D 4972)

- Organic Matter (T 267)

- Soluble Salts (EC1:2 (V:V)

4		TEST RESULTS SUBMISSION

The sample information required in the “Material Sampling and Testing” shall be included in the outsource laboratory test report form when submitted to the Administration.

Results for each test listed in the TESTING PROCEDURES shall be included on the submitted test report.

A copy of the landscaping soil test results shall be submitted to SATD at the following address:

Dr. Intikhab Haider

Office of Materials Technology

Soils and Aggregate Technology Division

7450 Traffic Drive

Hanover, MD 21076

or

bknipe@mdot.maryland.gov

5	Quality Assurance Requirements

The administration will take two samples from the specified source and verify the test results as per requirements given in Tables 1 and 2. If a failure occurs in the first two samples a third sample will be obtained and tested. Failure to meet the MDOT SHA specification after testing on three samples of same product (topsoil/BSM) may result in delisting of that product and/or producer from the list. If the first two samples fail, that stockpile cannot be used until it is modified.

At the time of sampling, the producer should keep split samples for verification testing, if needed. The producer may use any independent laboratory approved by MDOT  SHA as given in Section 2.1.2: Material Testing and Sampling, for verification of test results.

Table 1: Furnished Topsoil Test Value Specifications

| COMPOSITION – FURNISHED TOPSOIL |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| TEST PROPERTY | TEST 1 METHOD | TEST VALUE AND AMENDMENT |  |  |  |
| Prohibited Weeds | — | Free of live stems and roots of species in 920.01.01 as well as live stems and roots of Bermuda grass, Quack grass, and Yellow Nutsedge. |  |  |  |
| Debris | — | 1.0 % or less by weight of cement, concrete, asphalt, crushed gravel or construction debris when inspected. |  |  |  |
| Grading Analysis | R-58 | Sieve Size |  | Passing by Weight Minimum % |  |
|  |  | 2 in. |  | 100 |  |
|  |  | No. 4 |  | 90 |  |
|  |  | No. 10 |  | 80 |  |
| Textural Analysis | T-88 | Particle |  | % Passing by Weight |  |
|  |  | Size | mm | Minimum | Maximum |
|  |  | Sand | 2.0 – 0.050 | 20 | 75 |
|  |  | Silt | 0.050 – 0.002 | Combined Silt and Clay 25 | 75 |
|  |  | Clay | less than 0.002 |  | 30 |
| Soil pH | ASTM D 4972 | pH 6.1 to pH 7.4 |  |  |  |
| Organic Matter | T-267 | 4.0 to 8.0% OM by weight |  |  |  |
| Nutrient Content | — | Administration will assess. Apply fertilizer per NMP for nitrogen requirement and optimum fertility index values (FIV) for phosphorus and potassium. |  |  |  |
| Soluble Salts | EC 1:2(V:V) | 500 ppm (0.78 mmhos/cm) or less. |  |  |  |
| Harmful Materials | — | Topsoil shall not contain substances in concentrations that are harmful to human health, water quality, or plant growth. Industrial waste such as ash, slag, raw sludge, or similar materials shall not be soil components. |  |  |  |

Table 2: Bioretention Soil Mix Test Value Specifications

| COMPOSITION- BIORETENTION SOIL MIX (BSM) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TEST PROPERTY | TEST 1 METHOD | TEST VALUE |  |  |  |  |  |
| Weeds | — | Free of seed and viable plant parts of species in 920.06.02(a)(b)(c) when inspected. |  |  |  |  |  |
| Debris | — | No observable content of cement, concrete, asphalt, crushed gravel or construction debris. |  |  |  |  |  |
| Hardwood Mulch | — | 20% of the loose volume of BSM when inspected. |  |  |  |  |  |
| Textural Analysis | T-88 | Particle |  | % Passing by Weight |  |  |  |
|  |  | Size | mm | Minimum | Maximum |  |
|  |  | Sand | 2.0 – 0.050 | 79 | 94 |  |
|  |  | Silt | 0.050 – 0.002 | 4 | 20 | Combined Silt and Clay 21 |
|  |  | Clay | less than 0.002 | 1 | 10 |  |
| Soil pH | ASTM D4972 | pH of 5.7 to 7.4. |  |  |  |  |  |
| Organic Matter | T-267 | Minimum 1.5 % by weight. |  |  |  |  |  |
| Soluble Salts | EC 1:2(V:V) | 500 ppm (0.78 mmhos/cm) or less. |  |  |  |  |  |
| Harmful Materials | — | 920.01.01(a). |  |  |  |  |  |

- PROCESS FLOW CHARTS

6.1	Landscaping Producer Annual Eligibility Testing Process

Producer submits request to MDOT SHA

MDOT SHA responds to Producer within 10 working days with required documents

Producer collects and submits sample per Section 2.1.2 of this document and submits to Independent (SHA-Approved Lab) lab for testing

Producer submits Independent Lab test results and all worksheets/supporting documentation. See section 6.2

MDOT SHA responds to Producer within 5 working days with status of eligibility

Producer submits independent lab test results to SATD

No

Producer will be notified that the test results do not meet the specifications in Section 920

Producer will be notified that they will be included on the Eligibility list until the next submittal period

Yes

SATD Reviews Test Results

Do the test results meet the specification in Section 920?

6.2	Producers Eligibility

6.3	Addressing Failures with Administration QA Testing

Does QA sample meet the specification in Section 920?

Yes

LPD shall send SATD the NMP. NMP will be valid for 6 months. SATD will forward NMP to the projects and producer through Source of Supply Request submitted in MMS

Forward test results to LPD to develop an NMP

No

Is this the Second Failure?

Is this the First Failure?

If the product from a producer fails the split sample testing, the producer will be notified that they will be removed from the eligibility list until the next submittal period.

No

No

Yes

Yes

The producer will be asked to perform testing on Split samples for verification. Samples will go to producer’s lab of choice, which is on the approved lab list.

OMT will do perform testing on second sample. on second sample

- LANDSCAPING SOIL TESTING FREQUENCY

The frequency of testing landscaping soils shall be in accordance with Table 3.

Table 3: Landscaping Soil Testing Frequency

| Bi-annual | Sampling Month | NMP Prep. Month | NMP Expiration | Publication Date |
| --- | --- | --- | --- | --- |
| 1 | January/February | February/March | September 30th | March 31st |
| 2 | July/August | August/September | March 31st | September 30th |

# Appendix A

Landscaping Soil Producer’s Information

Office of Materials Technology

# Soils and Aggregate Technology Division

# Landscaping Soil Producer’s Information Sheet

# Name of Organization (Producer):

________________________________________________________________________

# Office / Facility (Subsidiary Landscaping Soils Producer):   Same as above ____             or   _____________________________________________________________________

Supervising Office’s Mailing Address:

# Street or P.O. Box:	_________________________________________

# Town / City:	_______________________________________________

# State:		_________________	 Zip:	_________________

# E-Mail Address:	_______________________________________________

# Phone No(s):		_______________________   _______________________

# Fax No.:		_______________________

# Stockpile Location (Name, If Applicable):	___________________________________

# Street or P.O. Box:	_______________________________________________

# Town / City:	__________________________ State: _______ Zip:  __________

Entitled Point of Contact:____________________________________________

# Title / Position:____________________________________________________

# E-Mail Address:____________________________________________________

# Phone No(s):	_______________________     ______________________

# Fax No.:	____________________

# Landscaping Soil to supply(s): Topsoil____ BSM _____

Do you want this location to be listed on the Eligibility List on MD Roads?  Yes _____   No _____

# Stockpile Location (Name, If Applicable):	___________________________________

# Street or P.O. Box:	_______________________________________________

# Town / City:	__________________________ State: _______ Zip:  __________

Entitled Point of Contact:	_________________________________________

# Title / Position:		_________________________________________

# E-Mail Address:	_______________________________________________

# Phone No(s):		_______________________     ______________________

# Fax No.:	____________________

# Landscaping Soil to supply(s): Topsoil____ BSM _____

Do you want this location to be listed on the Eligibility List on MD Roads?  Yes _____   No _____

Note:  Shaded areas will be published on-line.